20.12.2022

Network 01:

The network was grown in a solution of sulfolane, with 0.5 mM TBAPF6 and 12 mM EDOT on a PDMS film (Gel-Pak PF-40-X0) by applying a step function with an Agilent 33600A waveform generator (Vpp = 15 V through 25 V, f = 1 Hz through 10 Hz, Offset = none, Duty cycle = 50%) to the two gold electrodes (diameter = 24 μ).

After the network was grown and connected (based on visual inspection via a microscope), an sinusoidal potential (f = 10 Hz, Vpp = 300 mV) was applied to the gold electrodes with the Agilent 33600A waveform generator. The current through the network was measured with a current-voltage amplifier (Femto DLPCA-200) and an oscilloscope (Rohde & Schwarz HMO3004).

AC: 10Hz, 300mV

The current was also measured while the network with the solution and the PDMS film were acoustically excited with a home-made oscillator driven by Agilent 33220A waveform generator (sinusoidal potential with f = 50 Hz and Vpp = 2 V).

Excitation: 50Hz, 2V

The switches of the current-voltage amplifier were set to GND, 10e6 L, 10 Hz, AC.

DLPCA-200 (GND, 10^6L, 10 Hz, AC)

Oscilloscope settings: 20221220_02_Osc_SETTINGS.SCP

Measurements:

- No acoust. excitation: 20221220_01_10Hz_300mV-NoEx.CSV

- Acoust. excitation (50Hz, 1V): 20221220_01_10Hz_300mV-Ex50Hz_2V.CSV

Network 02:

Same procedure as for network 01:

Solution: Sulfolane, 0.5 mM TBAPF6, 12 mM EDOT

AC: 10Hz, 300mV

Acoustic excitation: 50Hz, 2V

DLPCA-200 (GND, 10^6L, 10 Hz, AC)

Initial network resistance: 180 kΩ

Oscilloscope settings: 20221220_02_Osc_SETTINGS.SCP

Measurements:

- No acoust. excitation: 20221220_02_10Hz_300mV-NoEx(1).CSV

- Acoust. excitation (50Hz, 1V): 20221220_02_10Hz_300mV-Ex50Hz_1V(1).CSV

- No acoust. excitation: 20221220_02_10Hz_300mV-NoEx(2).CSV

- Acoust. excitation (50Hz, 1V): 20221220_02_10Hz_300mV-Ex50Hz_1V(2).CSV

- No acoust. excitation: 20221220_02_10Hz_300mV-NoEx(3).CSV

21.12.2022

Network 03:

Same procedure as for network 01:

Solution: Sulfolane, 0.5 mM TBAPF6, 50 mM EDOT

AC: 20Hz, 300mV

Acoustic excitation: 50Hz, 1.5V

DLPCA-200 (GND, 10^5L, 10 Hz, AC)

Initial network resistance: 400 kΩ

Oscilloscope settings: 20221221_03_Osc_SETTINGS.SCP

Measurements:

- No acoust. excitation: 20221221_03_20Hz_300mV-NoEx(1).CSV

- Acoust. excitation (50Hz, 1.5V): 20221221_03_20Hz_300mV-Ex50Hz_1.5V(1).CSV

- No acoust. excitation: 20221221_03_20Hz_300mV-NoEx(2).CSV

- Acoust. excitation (50Hz, 1.5V): 20221221_03_20Hz_300mV-Ex50Hz_1.5V(1).CSV

- No acoust. excitation: 20221221_03_20Hz_300mV-NoEx(3).CSV

70kOhm no response

1.2 MOhm no response

50 MOhm no response

10kOhm weak response

7.9 kOhm  no response

Network 04:

Same procedure as for network 01:

Solution: Sulfolane, 0.5 mM TBAPF6, 50 mM EDOT

AC: 20Hz, 300mV

Acoustic excitation: 50Hz, 1.5V

DLPCA-200 (GND, 10^5L, 10 Hz, AC)

Initial network resistance: 17 kΩ

Oscilloscope settings:

Measurements:

17 kOhm

100: 1 Hz/300mV  - off

17: 1 Hz/300mV – 50 Hz/1.5V

18: 1 Hz/300mV – off

19: 10 Hz/300mV –  off

20:10Hz’/300mV – 50 Hz/1.5V

21: 10 Hz/300mV –  off

22: 15  Hz/300mV –  off

23: 15  Hz/300mV – 50 Hz/1.5V

24: 15  Hz/300mV –  off

25: 20  Hz/300mV –  off

26: 20  Hz/300mV – 50 Hz/1.5V

27: 20  Hz/300mV –  off

28: 30  Hz/300mV –  off

29: 30  Hz/300mV – 50 Hz/1.5V

30: 30  Hz/300mV –  off

31: 40  Hz/300mV –  off

32: 40  Hz/300mV – 50 Hz/1.5V

33: 40  Hz/300mV –  off

34: 50  Hz/300mV –  off

35: 50  Hz/300mV – 50 Hz/1.5V

36: 50  Hz/300mV –  off

37: 50  Hz/300mV –  off

38: 50  Hz/300mV – 50 Hz/1.5V

39: 50  Hz/300mV –  off

23.12.2022

Network 05:

Same procedure as for network 01:

Solution: Sulfolane, 0.5 mM TBAPF6, 50 mM EDOT

Impedance measurement with Autolab: 01_20221223_05_Sulf_0.5_10_woBios.xlsx

Initial network resistance: 50 kΩ

AC: 10Hz, 300mV

Acoustic excitation: 50Hz, 2V and 10 Hz/2V

DLPCA-200 (GND, 10^3L, 10 Hz, AC)

No response on oscilloscope

Network 06:

Same procedure as for network 01:

Solution: Sulfolane, 0.5 mM TBAPF6, 50 mM EDOT

Impedance measurement with Autolab:

Initial network resistance: 3 Ω

AC: 10Hz, 300mV

Acoustic excitation: 50Hz, 2V and 10 Hz/2V

DLPCA-200 (GND, 10^3L, 10 Hz, AC)

No response on oscilloscope

Network 07:

Same procedure as for network 01:

Solution: Sulfolane, 0.5 mM TBAPF6, 50 mM EDOT

Impedance measurement with Autolab

03.01.2023

Network 08:

Same procedure as for network 01:

Solution: Sulfolane, 0.5 mM TBAPF6, 50 mM EDOT

AC: 1Hz, 300mV

Acoustic excitation: 50Hz, 2V

DLPCA-200 (GND, 10^6L, 10 Hz, AC)

Network 09:

Same procedure as for network 01:

Solution: Sulfolane, 0.5 mM TBAPF6, 50 mM EDOT

Impedance measurements with Autolab: 01_20230103_09_Sulf_0.5_10

Oscilloscope measurements:

DLPCA-200 (GND, 10^6L, 10 Hz, AC)

Oscilloscope settings: SETTIN01.SCP

- No acoust. excitation (AC: 1Hz at 300mV): 20230103_09_1Hz_300mV-NoEx(1).CSV

- Acoust. excitation (AC: 1Hz at 300mV, acoust. Excit: 50Hz, 2V): 20230103_09_1Hz_300mV -Ex50Hz_2V(1).CSV

- No acoust. excitation (AC: 1Hz at 300mV): 20230103_09_1Hz_300mV-NoEx(2).CSV

- Acoust. excitation (AC: 1Hz at 300mV, acoust. Excit: 50Hz, 2V): 20230103_09_1Hz_300mV -Ex50Hz_2V(2).CSV - 10

- No acoust. excitation (AC: 1Hz at 300mV): 20230103_09_1Hz_300mV-NoEx(3).CSV

- No acoust. excitation (AC: 1Hz at 300mV): 20230103_09_1Hz_300mV-NoEx(4).CSV

- Acoust. excitation (AC: 1Hz at 300mV, acoust. Excit: 50Hz, 3V): 20230103_09_1Hz_300mV -Ex50Hz_3V(1).CSV

- No acoust. excitation (AC: 1Hz at 300mV): 20230103_09_1Hz_300mV-NoEx(5).CSV

- Acoust. excitation (AC: 1Hz at 300mV, acoust. Excit: 50Hz, 3V): 20230103_09_1Hz_300mV -Ex50Hz_3V(2).CSV

- No acoust. excitation (AC: 1Hz at 300mV): 20230103_09_1Hz_300mV-NoEx(6).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(1).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 2V): 20230103_09_10Hz_300mV -Ex50Hz_2V(1).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(2).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 2V): 20230103_09_10Hz_300mV -Ex50Hz_2V(2).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(3).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(4).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 3V): 20230103_09_10Hz_300mV -Ex50Hz_3V(1).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(5).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 3V): 20230103_09_10Hz_300mV -Ex50Hz_3V(2).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(6).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(7).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 3V): 20230103_09_10Hz_300mV -Ex50Hz_3V(3).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(8).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 3): 20230103_09_10Hz_300mV -Ex50Hz_3V(4).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(9).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(10).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 4V): 20230103_09_10Hz_300mV -Ex50Hz_4V(1).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(11).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 4): 20230103_09_10Hz_300mV -Ex50Hz_4V(2).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(12).CSV

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 4): 20230103_09_10Hz_300mV -Ex50Hz_4V(3).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(13).CSV

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(14).CSV  -39

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 1V): 20230103_09_10Hz_300mV -Ex50Hz_1V(1).CSV -40

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(15).CSV   - 41

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 2): 20230103_09_10Hz_300mV -Ex50Hz_2V(3).CSV - 42

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(16).CSV  - 43

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 3): 20230103_09_10Hz_300mV -Ex50Hz_3V(5).CSV - 44

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(17).CSV  -45

- Acoust. excitation (AC: 10 Hz at 300mV, acoust. Excit: 50Hz, 4): 20230103_09_10Hz_300mV -Ex50Hz_4V(3).CSV - 46

- No acoust. excitation (AC: 10Hz at 300mV): 20230103_09_10Hz_300mV-NoEx(18).CSV  - 47

It appears that the network does not respond to acoustic excitation anymore.

Impedance measurements with Autolab: 01_20230103_09_Sulf_0.5_10(2)

05.01.2023

Network 10:

1) AC current measurements (10 Hz, 300 mV) through a free-standing film (diameter: 5mm) made from a solution of sulfolane, with 0.5 mM TBAPF6 and 12 mM EDOT via two gold-wire electrodes (distance: approx.: 1.5 – 2 mm), a DLPCA-200 current-voltage amplifier (Ground, 10e6L,10Hz, AC) and a oscilloscope (Rohde&Schwarz HMO3004). The AC potential was generated by a function generator (Agilent 33600A). The current was measure without acoustic excitation and with acoustic excitations (50Hz/1.5V, 25Hz/1V,10Hz/1V, 10Hz/1.5V, 1Hz/1V, 1Hz/1.5V). The acoustic excitations were generated by the white oscillator.

Result: Acoustic excitation did not affect the AC current.

2) Some procedure as described in 1) but with slight fiber growth from the gold electrodes and acoustic exciations (50Hz/1.5V, 25Hz/1V,10Hz/1V, 10Hz/1.5V, 1Hz/1V, 1Hz/1.5V).

Result: Acoustic excitation did not affect the AC current.

The network was grown in a solution of sulfolane, with 0.5 mM TBAPF6 and 50 mM EDOT on a PDMS film (Gel-Pak PF-40-X0) by applying a step function with an Agilent 33600A waveform generator (Vpp = 15 V through 25 V, f = 1 Hz through 10 Hz, Offset = none, Duty cycle = 50%) to the two gold electrodes (diameter = 24 μ).

06.01.2023

Network 11:

Network 12:

A PEDOT network was grow in a free-standing film (diameter: 5mm) made from a solution of sulfolane, with 0.5 mM TBAPF6 and 12 mM EDOT with two gold-wire electrodes (distance: approx.: 1.5 – 2 mm). The growth parameters were f = 5 Hz, Vpp = 300-800 mV.

1) The AC current through the network was measured with a DLPCA-200 current-voltage amplifier and an oscilloscope (Rohde&Schwarz HMO3004). The AC current was generated with a wave function generator (Agilent 33600A).

a)	Acoustic excitation of film/network at 50 Hz and 810 mV

AC potential: 10 Hz at 300 mV

DLPCA-200 settings: GND, 10e6L, 10 Hz, DC

b)	Acoustic excitation of film/network at 25 Hz and 790 mV

AC potential: 10 Hz at 300 mV

DLPCA-200 settings: GND, 10e6L, 10 Hz, DC

c)	Acoustic excitation of film/network at 5 Hz and 850 mV

AC potential: 10 Hz at 300 mV

DLPCA-200 settings: GND, 10e6L, FBW, DC

c)	Acoustic excitation of film/network at 100 Hz and 3.1 V

AC potential: 10 Hz at 300 mV

DLPCA-200 settings: GND, 10e6L, FBW, DC

2) The impedance of the network was measured with an Autolab spectrometer for various excitation frequencies.

10.01.2023

Network 13:

A PEDOT network was grow in a free-standing film (diameter: 5mm) made from a solution of sulfolane, with 0.5 mM TBAPF6 and 12 mM EDOT with two gold-wire electrodes (distance: approx.: 1.5 – 2 mm). The growth parameters were f = 5-10 Hz, Vpp = 300-800 mV.

A probe potential of 100 mV DC was applied to the network with an Agilent 33600A waveform generator. The resulting current was measured with a DLPCA-200 current-voltage amplifier (GND, 10e6L, FBW, DC) connected to an oscilloscope (Rohde&Schwarz HMO3004).

During the measurement, a pair of scissors was dropped on the table on which the measurement setup was located from a height of approx. 5 cm and we blew slightly in the direction of the network.

Network 14:

A PEDOT network was grow in a free-standing film (diameter: 5mm) made from a solution of sulfolane, with 0.5 mM TBAPF6 and 12 mM EDOT with two gold-wire electrodes (distance: approx.: 1.5 – 2 mm). The growth parameters were f = 5-10 Hz, Vpp = 300-800 mV.

A probe potential of 100 mV DC was applied to the network with an Agilent 33600A waveform generator. The resulting current was measured with a DLPCA-200 current-voltage amplifier (GND, 10e6L, FBW, DC) connected to an oscilloscope (Rohde&Schwarz HMO3004).

The film and network were acoustically excited using a wave function generator in the following way:

- Acoustic excitation potential: step function, Vpp = 720 mV, f = 500 mHz, duty cycle = 80%

- Acoustic excitation potential: step function, Vpp = 720 mV, f = 500 mHz, duty cycle = 50%

- Acoustic excitation potential: Vpp = 720 mV, f = 500 mHz, duty cycle = 80%, step function followed by no excitation followed by sinusoidal function

22.02.2023

Network 20:

A PEDOT network was grow in a free-standing film made from a solution of sulfolane, with 0.5 mM TBAPF6 and 12 mM EDOT with two gold-wire electrodes. The growth parameters are unknown as the network was grown accidentally.

A probe potential was applied to the network with an Agilent 33600A waveform generator. The resulting current was measured with a DLPCA-200 current-voltage amplifier connected to an oscilloscope (Rohde&Schwarz HMO3004).

Resistance of network: 5 kΩ

- DLPCA-200 settings: GND, 105, L, FBW, DC; Rohde&Schwarz HMO3004 settings: DC, 50 Ω

| Probe potential (mV) | Probe potential shape | Probe frequency (Hz) | Oscillator potential (mV) | Oscillator potential shape | Oscillator frequency (Hz) | Data file name | DC (V) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 100 | Step | 0.001 | 100 | Sin | Knock on table | Sul01 |  |
| 100 | Step | 0.001 | 100 | Sin | 0 | Sul02 | 1.3 |
| 100 | Step | 0.001 | 100 | Sin | 1 | Sul03 | 1.1 |
| 100 | Step | 0.001 | 100 | Sin | 5 | Sul04 | 1.06 |
| 100 | Step | 0.001 | 100 | Sin | 10 | Sul05 | 0.98 |
| 100 | Step | 0.001 | 100 | Sin | 20 | Sul06 | 0.94 |
| 100 | Step | 0.001 | 100 | Sin | 30 | Sul07 | 0.92 |
| 100 | Step | 0.001 | 100 | Sin | 50 | Sul08 | 0.94 |
| 100 | Step | 0.001 | 100 | Sin | 75 | Sul09 | 1.1 |
| 100 | Step | 0.001 | 100 | Sin | 100 | Sul10 | 1.3 |
| 100 | Step | 0.001 | 100 | Sin | 25 | Sul11 | 920 |
| 100 | Step | 0.001 | 100 | Sin | 0.5 | Sul12 | 1.1 |
| 100 | Step | 0.001 | 100 | Step | 0.5 | Sul13 | 1.1 |
| 100 | Step | 0.001 | 100 | Step | 1 | Sul14 | 1.1 |
| 100 | Step | 0.001 | 100 | Step | 5 | Sul15 | 0.98 |
| 100 | Step | 0.001 | 100 | Step | 10 | Sul16 | 0.94 |
| 100 | Step | 0.001 | 100 | Step | 20 | Sul17 | 0.92 |
| 100 | Step | 0.001 | 100 | Step | 25 | Sul18 | 0.91 |
| 100 | Step | 0.001 | 100 | Step | 30 | Sul19 | 0.9 |
| 100 | Step | 0.001 | 100 | Step | 50 | Sul20 | 0.9 |
| 100 | Step | 0.001 | 100 | Step | 75 | Sul21 | 1.14 |
| 100 | Step | 0.001 | 100 | Step | 100 | Sul22 | 1.18 |

- DLPCA-200 settings: GND, 104, L, FBW, DC; Rohde&Schwarz HMO3004 settings: DC, 50 Ω

| Probe potential (mV) | Probe potential shape | Probe frequency (Hz) | Oscillator potential (mV) | Oscillator potential shape | Oscillator frequency (Hz) | Data file name | DC (V) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 100 | Step | 0.001 | 100 | Sin | 0 | Sul23 |  |
| 100 | Step | 100 | 100 | Step | 0.5 | Sul24 |  |
| 100 | Step | 100 | 100 | Step | 1 | Sul25 |  |
| 100 | Step | 100 | 100 | Step | 5 | Sul26 |  |
| 100 | Step | 100 | 100 | Step | 10 | Sul27 |  |
| 100 | Step | 100 | 100 | Step | 20 | Sul28 |  |
| 100 | Step | 100 | 100 | Step | 25 | Sul29 |  |
| 100 | Step | 100 | 100 | Step | 50 | Sul30 |  |
| 100 | Step | 100 | 100 | Step | 75 | Sul31 |  |
| 100 | Step | 100 | 100 | Step | 100 | Sul32 |  |
| 100 | Step | 100 | 100 | Sin | 0.5 | Sul33 |  |
| 100 | Step | 100 | 100 | Sin | 1 | Sul34 |  |
| 100 | Step | 100 | 100 | Sin | 5 | Sul35 |  |
| 100 | Step | 100 | 100 | Sin | 10 | Sul36 |  |
| 100 | Step | 100 | 100 | Sin | 20 | Sul37 |  |
| 100 | Step | 100 | 100 | Sin | 25 | Sul38 |  |
| 100 | Step | 100 | 100 | Sin | 50 | Sul39 |  |
| 100 | Step | 100 | 100 | Sin | 75 | Sul40 |  |
| 100 | Step | 100 | 100 | Sin | 100 | Sul41 |  |
| 100 | Step | 10 | 100 | Sin | 0 | Sul42 |  |
| 100 | Step | 10 | 100 | Sin | 5 | Sul43 |  |
| 100 | Step | 10 | 100 | Sin | 10 | Sul44 |  |
| 100 | Step | 10 | 100 | Sin | 20 | Sul45 |  |
| 100 | Step | 10 | 100 | Sin | 25 | Sul46 |  |
| 100 | Step | 10 | 100 | Sin | 50 | Sul47 |  |
| 100 | Step | 10 | 100 | Sin | 75 | Sul48 |  |
| 100 | Step | 10 | 100 | Sin | 100 | Sul49 |  |

07.03.2023

Network 21:

A PEDOT network was grow in a free-standing film made from a solution of sulfolane, with 1 mM TBAPF6 and 50 mM EDOT with two gold-wire electrodes. Growth parameters: Step potential of Vpp=500 mV with f = 10 Hz.

A probe potential was applied to the network with an Agilent 33600A waveform generator. The resulting current was measured with a DLPCA-200 current-voltage amplifier connected to an oscilloscope (Rohde&Schwarz HMO3004).

a) Impedance measurements:

01: Vrms`=0.3 V without probe potential and acoustic excitation: 21_Imp_01_Sulf_1mM_50mM_Vp=0_Vax=0

02: Vrms`=0.3 V without probe potential and an acoustic excitation with a step potential of Vax=50 mV, fax=25 Hz, 50% duty cycle: 21_Imp_02_Sulf_1mM_50mM_Vp=0_Vax=50mV_fax=25Hz

03: Vrms`=0.3 V without probe potential and acoustic excitation: 21_Imp_03_Sulf_1mM_50mM_Vp=0_Vax=0

04: Vrms`=0.3 V without probe potential and an acoustic excitation with a step potential of Vax=50 mV, fax=10 Hz, 50% duty cycle: 21_Imp_04_Sulf_1mM_50mM_Vp=0_Vax=50mV_fax=10Hz

05: Vrms`=0.3 V without probe potential and acoustic excitation: 21_Imp_05_Sulf_1mM_50mM_Vp=0_Vax=0

b) Resistance per multimeter: 60 kΩ

c) Current-through-network measurement

01: 	Probe potential: 300 mV DC

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω, 100mV per grid

Result: Knocking on table did not affect the current

02: 	Probe potential: 300 mV DC

Acoustic excitation: none

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B01

03: 	Probe potential: 300 mV DC

Acoustic excitation: fax = 10Hz, Vax= 50 mV

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B02, 03

04: 	Probe potential: 300 mV DC

Acoustic excitation: fax = 25Hz, Vax= 50 mV

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B04, 05

05: 	Probe potential: sin, 300 mV, 50 Hz

Acoustic excitation: none

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 06

06: 	Probe potential: sin, 300 mV, 50 Hz

Acoustic excitation: fax = 25Hz, Vax= 50 mV

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 07

07: 	Probe potential: sin, 300 mV, 50 Hz

Acoustic excitation: fax = 50Hz, Vax= 50 mV

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 08

08: 	Probe potential: sin, 300 mV, 50 Hz

Acoustic excitation: fax = 5Hz, Vax= 50 mV

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 09

09: 	Probe potential: sin, 300 mV, 50 Hz

Acoustic excitation: fax = 1 Hz, Vax= 50 mV

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 10

10: 	Probe potential: sin, 300 mV, 50 Hz

Acoustic excitation: none

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 11

11: 	Probe potential: sin, 300 mV, 50 Hz

Acoustic excitation: fax = 1 Hz, Vax= 300 mV

DLPCA-200 settings: GND, 105, L, FBW, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 12

09.03.2023

Network 22:

01: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 1 Hz, Vax= 90 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B13

02: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 1 Hz, Vax= 90 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B14

03: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 2 Hz, Vax= 90 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B15

04: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, Vax= 90 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B16

05: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 25 Hz, Vax= 90 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B17

06: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 200 mHz, Vax= 90 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B18

07: 	Probe potential: 300 mV, 50 Hz

Acoustic excitation: fax = 2 Hz, Vax= 90 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B19

30.03.2023

Network 24:

01: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, Vax= 200 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 0 Ω

Result: B20

02: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 200 mHz, Vax= 300 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B21

03: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 200 mHz, Vax= 300 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B22

04: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 200 mHz, Vax= 300 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B23

05: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 200 mHz, Vax= 300 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B24

06: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 200 mHz, Vax= 290 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B25

07: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 400 mHz, Vax= 250 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B26

08: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 1 Hz, Vax= 200 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B27

09: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 5 Hz, Vax= 170 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: B28

03.05.2023

Network 34:

01: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 1 Hz, 200 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 234100M

Network 35:

01: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 300 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 234100N

02:	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 300 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 234100O

03:	Probe potential: DC, 300 mV

Acoustic excitation: fax = 0 Hz, 0 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 234100P

05.05.2023

Network 36:

01: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 200 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 2341002, resistance too high, no current visible in oscilloscope, first growth process

02: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 200 mV

DLPCA-200 settings: GND, 107, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 2341003, resistance too high, slight current visible in oscilloscope, second growth 	process

03: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 200 mV

DLPCA-200 settings: GND, 107, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 2341004, slightly more current visible in oscilloscope (still extremely low), third 	growth process

04: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 300 mV

DLPCA-200 settings: GND, 107, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 2341005, slightly more current visible in oscilloscope (still extremely low), fourth 	growth process, fibers very close to connecting

05: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 150 mV

DLPCA-200 settings: GND, 107, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 2341006, fibers likely disconnected before measurement

06: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 300 mV

DLPCA-200 settings: GND, 106, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: 2341007, fibers connected, ohmic behavior

10.05.2023

Network 37:

01: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 250 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC02

02: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 0 mHz, 0 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC03

03: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 300 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC04

04: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 500 mHz, 400 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC05

05: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 1 Hz, 200 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC06

06: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 1 Hz, 250 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC07

07: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 2 Hz, 250 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC08

08: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 5 Hz, 250 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC09

09: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 250 mHz, 250 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC10

10: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 100 mHz, 250 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC11

11: 	Probe potential: DC, 300 mV

Acoustic excitation: fax = 10 Hz, 250 mV

DLPCA-200 settings: GND, 105, L, 10Hz, DC;

Rohde&Schwarz HMO3004 settings: DC, 50 Ω

Result: TRC12

10.10.2023:

- Prepared 3 different solutions, all with 10ml Sulfolane as the solvent:

  - 1mM TBAPF6(3.874 mg), 50mM EDOT (53 μl measured with eppendorf pipette, comparison with water for better accuracy)

  - 0.5 mM TBAPF6 (1.937 mg), 50mM EDOT

  - 0.1 mM TBAPF6 (0.387 mg), 50mM EDOT

- 4th solution prepared with 50ml Sulfolane, 0.02 mM TBAPF6 (0.387 mg) and 50 mM EDOT (214 μl added to a solution already containing 53 μl, yielding 267 μl)

12.10.2023:

Network 39:

- Impedance measurements using the Autolab for different solutions:

  - 1_FRA_0mM_0mM_Sulfolane_0Hz_no_fibers
Pure Sulfolane

  - 2_FRA_0.02mM_50mM_Sulfolane_0Hz_no_fibers

Sulfolane with 0.02mM TBAPF6, 50mM EDOT

  - 3_FRA_0.02mM_50mM_Sulfolane_0Hz_no_fibers
Sulfolane with 0.02mM TBAPF6, 50mM EDOT

  - 4_FRA_0.1mM_50mM_Sulfolane_0Hz_no_fibers
Sulfolane with 0.1mM TBAPF6, 50mM EDOT

  - 5_FRA_no_solution
Air inbetween gold electrodes, no Solution used

  - 6_FRA_0.5mM_50mM_Sulfolane_0Hz_no_fibers
Sulfolane with 0.5mM TBAPF6, 50mM EDOT

  - 7_FRA_1mM_50mM_Sulfolane_0Hz_no_fibers
Sulfolane with 1mM TBAPF6, 50mM EDOT

  - 8_FRA_0mM_0mM_Sulfolane_0Hz_no_fibers
Pure Sulfolane

- Solution with 0.02mM TBAPF6 is used to grow thick PEDOT-film on 2 of the gold electrodes (frequency 1 μHz, amplitude 600-600mV times 50), picture „2x_growth_on_electrode“

- Growth in 0.02mM solution does not work even at 10V and 100mHz, pictures „electrode_during_growth_in_0.02mM_solution“, „after_removing_0.02mM_solution“

- 0.5mM solution used instead, 10Hz, 1V-1.2V (x50)
successful fiber growth, impedance measurement „9_FRA_0.5mM_50mM_Sulfolane_0Hz_fibers“

after connecting the BNC cables using a splitter, sudden strong growth occured, destroying the fiber network, see picture „after_connecting_BNC_cables“

13.10.2023:

Network 40:

- Fiber growth in 0.1mM solution, first growth on two electrodes to serve as gate: „growth_for_gate_1x“

- growth tried at 1Hz and 2V (x50) first → too high. Fibers disconnect from gold
around 1V-1.5V (x50) seems appropriate, duty cycle varied between 45-55%
→ fiber growth stops early, see „after_first_try_to_grow“
→ Impedance measurement btw fibers with PEDOT on them: 1_FRA_0.1mM_50mM_Sulfolane_0Hz_PEDOT_on_electrodes
→ solution changed against new 0.1mM solution, doesn’t work either
→ solution changed to 0.5mM (10Hz, 1V, 50%) → immediate growth, salt concentration might be an issue → multiple connections, impedance measurement performed (0.1V): 2_FRA_0.5mM_50mM_Sulfolane_0Hz_fibers

- Sweep-Me measurements performed,

  - Transfer curves at -0.1, -0.3, -0.5, -0.7, -1 (same for plus) Vds and gate swept with 1s hold from -1V to 1V

  - same done with gate sweeping from -2 to 2V for larger area

  - output curves measured, sweeping Vds from -1 to 1V and back, gate varied in 0.2V steps from -2V to 2V, 1s hold

- Pictures of the network before and after the measurements were saved

- Impedance measurement after the measurements were performed: 3_FRA_0.5mM_50mM_Sulfolane_0Hz_fibers_after_SMU_measurements

19.10.2023:

Network 41:

- 0.5mM TBAPF6, 50mM EDOT solution used

- growth on gate electrode at 600 mV x50 and 1  μHz: „growth_on_gate_electrode_3x“

- growth at 10 Hz and 1V-1.2V (x50). First, growth btw gate and one electrode was observed until the gate was disconnected from the SMU. Afterwards, slow growth btw desired electrodes and connection after over 30 minutes: „network_after_growth_3x“

- Impedance measurement using Autolab, 0.1V: „1_FRA_0.5mM_50mM_Sulfolane_0Hz_fibers“, „2_FRA_0.5mM_50mM_Sulfolane_0Hz_fibers“

- SMU measurement: Current dominated by leak, up to 10^(-6) at over 1V V_ds.

- Tried to switch gate electrode → Disconnection → reconnected with 800mV: „network_after_reconnection_3x“ → new Impedance measurement → „3_FRA_0.5mM_50mM_Sulfolane_0Hz_fibers_reconnected“

- Retried SMU measurement with Gate electrode with way less growth on it

- looks much better, but switching at 1V Vds only after 2V Vg → Vg tested btw -1V and 3.5V

- leak is bad for on/off, but Vg of und 2.5V seems fine (ideal:2.3V) at 1V Vds

- same measurement a bit later suggests an ideal Vg of 1.7V

- leak is worse at negative Vds → use positive for measurement

- Vds then applied with wavefunction generator (Agilent 33600A, 1 μHz, 1V, polarity checked with multimeter), V_g applied with SMU

- acoustic signal started at 1Hz, 1V. More voltage than usually needed to visually see effect. Maybe oscillator is broken

- 10Hz01.csv saved with 1.7V Vg, 1V Vds and 1.5V acoustic excitation at 1Hz, no reaction, GND, 10^5, L, 10Hz, DC, Oscilloscope: DC, 50 Ohm

- 10Hz02.csv saved with 1V Vg, 1V Vds and 1.5V acoustic excitation at 1Hz, no reaction, GND, 10^5, L, 10Hz, DC, Oscilloscope: DC, 50 Ohm

- 10Hz03.csv saved with 1V Vg, 1V Vds and 1.5V acoustic excitation at 1Hz, no reaction, GND, 10^7, L, 10Hz, DC, Oscilloscope: DC, 50 Ohm

- 10Hz04.csv saved with -1V Vg, 1V Vds and 1.5V acoustic excitation at 1Hz, no reaction, GND, 10^6, L, 10Hz, DC, Oscilloscope: DC, 50 Ohm

- oscillator might have stopped inbetween

- 10Hz05.csv saved with 1.5V Vg, 1V Vds and 1.6V acoustic excitation at 1Hz, reaction, GND, 10^7, L, 10Hz, DC, Oscilloscope: DC, 50 Ohm

- 10Hz06.csv saved with 2V Vg, 1V Vds and 2.2V acoustic excitation at 1Hz, reaction, GND, 10^7, L, 10Hz, DC, Oscilloscope: DC, 50 Ohm

- 10Hz07.csv saved with 1.5V Vg, 1V Vds and 2.2V acoustic excitation at 1Hz, reaction, GND, 10^7, L, 10Hz, DC, Oscilloscope: DC, 50 Ohm

- fibers already broken in 10Hz07 measurement

25.10.2023:

Network 42:

- Gate electrode growt at 1μHz, 200mV (x50): “gate_electrode_growth_3x”

- fiber growth started at 10Hz and 1V (increased to 1.2V later) (x50): voltage drop exists btw all 4 electrodes (27V btw drain and source, but also gate and source) → growth not controllable to only happen btw 2 electrodes

- sudden growth spurts towards the end

- Impedance measurement at 100mV: „1_FRA_0.5mM_50mM_Sulfolane_0Hz_network“

- fibers broke during process of switching cable to SMU → reconnection .> Imepdance: „3_FRA_0.5mM_50mM_Sulfolane_0Hz_reconnected“

- network disconnected again, not sure, if it was disconnected during impedance measurement 3 → Impedance of disconnected network: 4_FRA_0.5mM_50mM_Sulfolane_0Hz_disconnected

- reconnected again at 600mV and 10Hz, left on for 2 minutes → Impedance: 5_FRA_0.5mM_50mM_Sulfolane_0Hz_reconnected_again

- SMU: extremely high leakage. At -0.5V basically no switching

- after a couple of tries, voltage applied to source instead of drain to check if geometry plays a role (best results so far at 1V Vds, on/off ratio: >10), no good results → switched back

- looped measurement at 1V Vds and -1 to 3V Vg → seems semi-stable. On forward loop, switching at around 1V but unstable, backward loop around 2.5V seems stable

- try acoustic measurements with 1V Vds and 2.6V Vg

- 100mV voltage at channel1 at 10^3 amplification, even though no voltage is applied yet. Multimeter shows 40mV between drain and source

- 1.5V at Osci with 10^3 amp when SMU is applied, overload of the pre-amp, SMU shows current in 10^-2 range

- network broke off

- setup is likely incorrect, current probably not through network