Supplementary material for Härtel, B., Jonkcheere, R., Wauschkuhn, B., Ratschbacher, L.: The closure temperature(s) of zircon Raman dating. Submitted to Geochronology.

Supplementary Table S1. Raman measurements of the isochronal annealing runs. Band positions (ω) and widths (Γ) are given as wavenumbers [cm-1] for seven Raman bands ( internal bands ν1(SiO4) to ν3(SiO4); the external rotation band (ER) at ~356 cm-1 and the external bands at ~200 cm-1).

| sample | T [°C] | ω1 | Γ1 | ω2 | Γ2 | ω3 | Γ3 | ωER | ΓER | ωe1 | Γe1 | ωe2 | Γe2 | ωe3 | Γe3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | unannealed | 969.19 | 8.52 | 436.81 | 13.16 | 1001.3 | 10.09 | 351.63 | 14.43 | 201.83 | 5.22 | 210.75 | 8.7 | 223.34 | 7.99 |
| 2 | unannealed | 968.66 | 9.6 | 436.91 | 14.65 | 1001.02 | 11.47 | 351.26 | 17.15 | 202.05 | 5.97 | 210.36 | 9.51 | 223.16 | 8.59 |
| 3 | unannealed | 969.17 | 10.52 | 436.7 | 13.63 | 1001.78 | 11.42 | 351.5 | 14.86 | 201.77 | 4.71 | 211.68 | 10.65 | 223.38 | 7.59 |
| 4 | unannealed | 967.42 | 12 | 436.04 | 18.6 | 999.33 | 14.03 | 349.71 | 20.07 | 201.65 | 5.92 |  |  | 222.79 | 10.02 |
| 5 | unannealed | 968.27 | 9.48 | 436.47 | 15.33 | 1000.37 | 11.95 | 351.11 | 17.29 | 201.67 | 5.5 | 209.92 | 10.08 | 222.87 | 8.93 |
| 6 | unannealed | 968.24 | 9.37 | 436.59 | 15.14 | 1000.44 | 11.04 | 350.94 | 16.06 | 201.87 | 5.34 | 210.06 | 10.79 | 223.08 | 8.71 |
| 7 | unannealed | 967.02 | 10.14 | 435.84 | 16.85 | 998.72 | 13.37 | 350.01 | 19.06 | 201.52 | 7.05 | 209.5 | 11.55 | 222.66 | 9.6 |
| 8 | unannealed | 967.63 | 10.06 | 436.38 | 16.16 | 999.78 | 12.49 | 350.64 | 18.59 | 201.82 | 6.37 | 209.48 | 11.01 | 222.78 | 9.41 |
| 1 | 600 | 970.54 | 8.47 | 435.22 | 12.82 | 1002.12 | 9.46 | 353.42 | 11.58 | 201.59 | 4.59 | 210.88 | 8.91 | 223.11 | 7.54 |
| 2 | 600 | 971.59 | 7.75 | 436.21 | 12.43 | 1003.8 | 8.56 | 354.29 | 10.24 | 201.81 | 3.52 | 211.28 | 9.03 | 223.49 | 6.76 |
| 3 | 600 | 970.8 | 9.19 | 435.71 | 13.91 | 1003.1 | 10.73 | 353.16 | 12.71 | 201.58 | 4.32 | 210.99 | 11.29 | 223.1 | 8.2 |
| 4 | 600 | 970.81 | 9.69 | 435.58 | 14.73 | 1003.25 | 10.91 | 353.54 | 13.2 | 201.73 | 4.93 | 210.81 | 13.21 | 223.03 | 8.52 |
| 5 | 600 | 971.55 | 7.29 | 436.04 | 12.26 | 1003.58 | 8.41 | 354.12 | 10.16 | 201.68 | 3.46 | 211.37 | 8.31 | 223.39 | 7.04 |
| 6 | 600 | 971.16 | 8.98 | 435.87 | 14.01 | 1003.42 | 9.81 | 353.89 | 11.7 | 201.76 | 4.47 | 210.69 | 10.2 | 223.22 | 7.99 |
| 7 | 600 | 971.13 | 9.91 | 436.04 | 13.73 | 1003.8 | 11.12 | 353.83 | 13.47 | 201.68 | 4.79 | 210.81 | 10.06 | 223.09 | 8.02 |
| 8 | 600 | 970.51 | 10.1 | 435.49 | 14.82 | 1002.54 | 11.04 | 353.56 | 13.52 | 201.68 | 4.61 | 210.29 | 12.39 | 223.15 | 7.94 |
| 1 | 700 | 971.87 | 7.49 | 436.16 | 11.29 | 1004.1 | 8.42 | 354.58 | 9.52 | 201.79 | 3.79 | 211.71 | 9 | 223.7 | 6.63 |
| 2 | 700 | 971.89 | 8.1 | 436.05 | 11.19 | 1004.26 | 9.39 | 354.68 | 10.39 | 201.78 | 3.78 | 211.46 | 9.55 | 223.54 | 6.52 |
| 3 | 700 | 971.57 | 8.21 | 435.95 | 11.77 | 1003.92 | 9.54 | 354.44 | 10.62 | 201.78 | 4.15 | 211.16 | 8.84 | 223.45 | 7.12 |
| 4 | 700 | 971.9 | 8.44 | 436.07 | 12.04 | 1004.5 | 9.36 | 354.82 | 10.2 | 201.83 | 4.05 | 211.06 | 9.57 | 223.4 | 7.33 |
| 5 | 700 | 972.27 | 6.95 | 436.29 | 11.4 | 1004.56 | 7.79 | 354.89 | 8.82 | 201.73 | 3.15 | 211.77 | 8.87 | 223.52 | 6.57 |
| 6 | 700 | 972.23 | 8.38 | 435.94 | 12.63 | 1004.53 | 8.6 | 354.96 | 9.51 | 201.84 | 3.79 | 211.44 | 10.35 | 223.4 | 7.27 |
| 7 | 700 | 971.8 | 8.45 | 436.11 | 11.61 | 1004.24 | 9.37 | 354.66 | 10.37 | 201.81 | 3.76 | 211.24 | 8.94 | 223.47 | 6.42 |
| 8 | 700 | 972.19 | 8.75 | 436 | 12.42 | 1004.67 | 9.22 | 355.17 | 10.2 | 201.82 | 4.1 | 211.1 | 10.06 | 223.35 | 7.46 |
| 1 | 800 | 972.5 | 6.35 | 436.51 | 10.32 | 1004.94 | 7.18 | 355.01 | 8.06 | 201.81 | 3.03 | 211.98 | 7.49 | 223.82 | 6.02 |
| 2 | 800 | 972.63 | 5.85 | 436.95 | 9.45 | 1005.44 | 7.26 | 355.09 | 7.67 | 201.81 | 2.75 | 212.05 | 6.83 | 223.9 | 5.6 |
| 3 | 800 | 972.73 | 6.09 | 436.97 | 9.36 | 1005.49 | 7.32 | 355.21 | 7.99 | 201.87 | 2.77 | 212.25 | 6.73 | 224.08 | 5.51 |
| 4 | 800 | 971.91 | 8.44 | 435.85 | 11.76 | 1004.09 | 9.12 | 354.52 | 9.81 | 201.85 | 3.77 | 211.1 | 9.74 | 223.48 | 7.41 |
| 5 | 800 | 972.39 | 6.99 | 436.48 | 9.86 | 1005.15 | 8.48 | 354.88 | 8.76 | 201.74 | 3.32 | 211.78 | 8.56 | 223.65 | 6.34 |
| 6 | 800 | 971.98 | 7.21 | 435.84 | 10.91 | 1003.94 | 7.63 | 354.54 | 9.13 | 201.74 | 3.14 | 211.67 | 9.79 | 223.57 | 6.57 |
| 7 | 800 | 971.32 | 7.9 | 435.22 | 11.49 | 1003.27 | 8.96 | 353.63 | 9.38 | 201.67 | 3.26 | 212.78 | 14.41 | 223.52 | 6.52 |
| 8 | 800 | 972.18 | 7.44 | 435.76 | 11 | 1004.5 | 8.46 | 354.65 | 8.8 | 201.78 | 3.34 | 212.1 | 10.93 | 223.55 | 6.69 |
| 3 | 900 | 972.77 | 4.09 | 437.55 | 7.44 | 1005.28 | 5.68 | 354.77 | 6.96 | 201.9 | 1.98 | 212.9 | 4.43 | 224.42 | 4.42 |
| 4 | 900 | 972.47 | 6.64 | 436.57 | 9.39 | 1004.76 | 7.7 | 354.88 | 8.63 | 202.02 | 2.98 | 212.22 | 8.39 | 224.05 | 6.2 |
| 7 | 900 | 972.6 | 4.94 | 437.04 | 8.46 | 1005.11 | 6.78 | 354.81 | 7.49 | 201.92 | 2.45 | 212.48 | 5.72 | 224.19 | 5.14 |
| 8 | 900 | 972.64 | 5.94 | 436.79 | 9.02 | 1005.18 | 7.03 | 355.14 | 7.61 | 201.95 | 2.69 | 212.19 | 6.81 | 224.07 | 5.74 |
| 3 | 1000 | 972.38 | 3.78 | 437.1 | 7.68 | 1004.7 | 5.01 | 354.13 | 6.72 | 201.65 | 2.01 | 212.65 | 4.42 | 224.09 | 4.54 |
| 4 | 1000 | 972.78 | 3.73 | 437.38 | 7.27 | 1005.38 | 5.26 | 354.52 | 6.44 | 201.63 | 1.91 | 212.79 | 4.45 | 224.09 | 4.36 |
| 7 | 1000 | 973.05 | 3.33 | 437.52 | 6.92 | 1005.76 | 4.96 | 354.98 | 6.19 | 201.64 | 1.85 | 212.86 | 3.91 | 224.17 | 4.12 |
| 8 | 1000 | 972.72 | 3.7 | 437.17 | 7.58 | 1005.2 | 5.16 | 354.64 | 6.72 | 201.66 | 2.02 | 212.75 | 4.49 | 224.14 | 4.53 |

Supplementary Table S2. Raman data of the isothermal annealing runs. Band positions (ω) and widths (Γ) are given as wavenumbers [cm-1] for seven Raman bands ( internal bands ν1(SiO4) to ν3(SiO4); the external rotation band (ER) at ~356 cm-1 and the external bands at ~200 cm-1).

| sampIe | t [min] | T [°C] | ω1 | Γ1 | ω2 | Γ2 | ω3 | Γ3 | ωer | Γer | ωe1 | Γe1 | ωe2 | Γe2 | ωe3 | Γe3 | Φ2 | Φ3 | ΦER |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 500 | 968.06 | 12.95 | 436.27 | 20.05 | 1000.36 | 14.74 | 350.26 | 23.32 | 201.90 | 7.81 | 213.61 | 23.75 | 222.88 | 11.53 | 0.00 | 0.00 | 0.00 |
| 1 | 10 | 500 | 969.52 | 10.01 | 436.27 | 15.13 | 1001.65 | 11.36 | 352.02 | 15.88 | 201.66 | 5.12 |  |  | 5.12 | 8.31 | 0.33 | 0.26 | 0.38 |
| 1 | 30 | 500 | 970.24 | 9.07 | 436.50 | 14.12 | 1002.31 | 10.93 | 352.93 | 13.96 | 201.83 | 4.26 |  |  | 223.34 | 7.82 | 0.39 | 0.30 | 0.47 |
| 1 | 90 | 500 | 969.85 | 10.07 | 436.02 | 15.21 | 1002.25 | 11.31 | 352.62 | 15.11 | 201.88 | 3.78 |  |  | 223.41 | 7.60 | 0.32 | 0.27 | 0.42 |
| 1 | 300 | 500 | 970.21 | 9.03 | 435.93 | 14.37 | 1002.61 | 10.29 | 353.07 | 13.42 | 201.76 | 4.40 |  |  | 223.21 | 7.54 | 0.38 | 0.35 | 0.50 |
| 1 | 1440 | 500 | 969.81 | 9.47 | 435.03 | 14.62 | 1001.30 | 10.68 | 352.54 | 13.79 | 201.54 | 4.36 | 210.97 | 13.99 | 222.85 | 8.38 | 0.36 | 0.32 | 0.48 |
| 2 | 0 | 500 | 968.95 | 22.13 | 435.33 | 21.27 | 999.68 | 14.71 | 348.25 | 26.08 | 201.71 | 8.55 | 211.36 | 9.57 | 222.57 | 12.52 | 0.00 | 0.00 | 0.00 |
| 2 | 10 | 500 | 968.90 | 12.47 | 435.88 | 16.92 | 1000.82 | 14.16 | 351.54 | 17.95 | 201.77 | 4.59 |  |  | 223.23 | 8.27 | 0.27 | 0.04 | 0.36 |
| 2 | 30 | 500 | 967.86 | 10.79 | 435.47 | 17.47 | 999.88 | 13.39 | 351.00 | 19.44 | 201.56 | 5.80 |  |  | 222.89 | 9.64 | 0.23 | 0.10 | 0.30 |
| 2 | 90 | 500 | 968.17 | 12.08 | 435.03 | 17.14 | 1000.01 | 13.54 | 350.74 | 17.11 | 201.70 | 4.57 |  |  | 222.98 | 8.66 | 0.25 | 0.09 | 0.40 |
| 2 | 300 | 500 | 970.56 | 10.26 | 435.97 | 14.39 | 1002.41 | 10.36 | 352.38 | 14.82 | 201.88 | 4.95 | 211.06 | 9.68 | 223.18 | 8.89 | 0.42 | 0.34 | 0.50 |
| 2 | 1440 | 500 | 970.39 | 11.22 | 435.12 | 14.08 | 1001.50 | 10.30 | 352.71 | 13.14 | 201.56 | 3.92 | 211.35 | 10.55 | 223.22 | 7.72 | 0.44 | 0.34 | 0.58 |
| 3 | 0 | 500 | 967.39 | 16.32 | 435.67 | 20.15 | 999.15 | 15.83 | 349.17 | 24.01 | 201.80 | 4.85 |  |  | 222.74 | 10.72 | 0.00 | 0.00 | 0.00 |
| 3 | 30 | 500 | 968.57 | 12.81 | 435.64 | 18.69 | 1000.57 | 14.66 | 351.43 | 20.16 | 201.66 | 4.89 |  |  | 223.18 | 9.57 | 0.10 | 0.08 | 0.19 |
| 3 | 90 | 500 | 968.86 | 13.70 | 435.58 | 18.65 | 1000.57 | 14.70 | 351.42 | 19.32 | 201.60 | 6.78 | 210.74 | 11.99 | 222.90 | 10.01 | 0.10 | 0.08 | 0.23 |
| 3 | 300 | 500 | 968.98 | 13.22 | 435.33 | 18.68 | 1000.86 | 14.38 | 351.69 | 19.06 | 201.57 | 6.76 | 210.52 | 12.35 | 222.93 | 10.00 | 0.10 | 0.10 | 0.24 |
| 3 | 1440 | 500 | 968.95 | 13.34 | 435.28 | 18.16 | 1000.85 | 14.00 | 351.99 | 18.36 | 201.54 | 6.69 | 210.19 | 13.01 | 222.72 | 10.06 | 0.13 | 0.13 | 0.28 |
| 4 | 0 | 500 | 967.36 | 13.53 | 435.86 | 18.70 | 999.14 | 15.11 | 349.12 | 22.22 | 201.62 | 5.95 |  |  | 223.13 | 10.33 | 0.00 | 0.00 | 0.00 |
| 4 | 10 | 500 | 967.72 | 11.81 | 434.68 | 19.51 | 998.63 | 13.95 | 350.26 | 18.02 | 201.40 | 6.46 | 211.18 | 13.60 | 222.48 | 10.04 | 0.00 | 0.09 | 0.23 |
| 4 | 30 | 500 | 968.66 | 12.84 | 435.76 | 18.88 | 1000.55 | 14.09 | 351.14 | 19.85 | 201.74 | 6.54 | 210.38 | 12.49 | 223.09 | 10.33 | 0.00 | 0.08 | 0.13 |
| 4 | 300 | 500 | 968.70 | 11.73 | 435.35 | 17.80 | 1000.81 | 13.97 | 351.64 | 18.27 | 201.43 | 6.38 | 210.13 | 14.57 | 222.70 | 10.05 | 0.07 | 0.09 | 0.21 |
| 4 | 1440 | 500 | 969.05 | 12.75 | 435.33 | 17.96 | 1000.88 | 13.81 | 351.93 | 17.91 | 201.63 | 6.53 | 210.40 | 12.57 | 222.84 | 10.02 | 0.05 | 0.10 | 0.23 |
| 5 | 0 | 600 | 963.23 | 20.45 | 435.95 | 0.00 | 995.82 | 23.76 | 345.71 | 35.73 | 202.05 | 13.63 | 209.39 | 5.64 | 220.81 | 18.33 | 0.00 | 0.00 | 0.00 |
| 5 | 10 | 600 | 967.19 | 10.63 | 435.95 | 0.00 | 999.21 | 19.23 | 350.10 | 24.64 | 201.52 | 9.83 |  |  | 222.98 | 11.51 | 0.00 | 0.21 | 0.35 |
| 5 | 30 | 600 | 967.97 | 14.04 | 435.95 | 28.46 | 1000.41 | 17.88 | 350.69 | 20.83 | 201.25 | 9.03 | 209.05 | 17.81 | 222.13 | 13.90 | 0.00 | 0.27 | 0.46 |
| 5 | 90 | 600 | 968.82 | 14.27 | 437.06 | 24.99 | 1001.52 | 16.51 | 351.43 | 19.13 | 202.45 | 12.64 | 210.90 | 7.57 | 222.01 | 15.77 | 0.00 | 0.33 | 0.52 |
| 5 | 300 | 600 | 968.69 | 11.68 | 436.78 | 23.55 | 1001.18 | 16.34 | 351.22 | 18.52 | 201.04 | 7.72 |  |  | 222.59 | 13.92 | 0.00 | 0.34 | 0.54 |
| 5 | 1440 | 600 | 968.25 | 12.36 | 436.33 | 22.37 | 1000.49 | 16.54 | 351.17 | 19.51 | 201.73 | 9.38 | 210.16 | 11.09 | 222.29 | 13.64 | 0.00 | 0.33 | 0.50 |
| 5 | 7200 | 600 | 969.06 | 10.04 | 436.91 | 19.22 | 1001.76 | 14.39 | 351.87 | 17.52 | 201.81 | 10.40 | 210.39 | 9.52 | 222.10 | 12.37 | 0.00 | 0.43 | 0.57 |
| 6 | 0 | 600 | 965.94 | 20.75 | 434.77 | 28.99 | 997.12 | 19.05 | 347.82 | 29.06 | 201.96 | 9.96 | 207.00 | 24.95 | 222.72 | 12.79 | 0.00 | 0.00 | 0.00 |
| 6 | 10 | 600 | 967.37 | 11.97 | 434.77 | 0.00 | 1000.19 | 18.77 | 350.05 | 25.13 | 201.89 | 12.51 | 215.39 | 13.17 | 222.72 | 13.84 | 0.00 | 0.02 | 0.15 |
| 6 | 90 | 600 | 968.36 | 11.94 | 435.11 | 21.23 | 1000.20 | 14.62 | 351.42 | 19.75 | 201.84 | 4.45 |  |  | 222.93 | 11.70 | 0.32 | 0.26 | 0.37 |
| 6 | 300 | 600 | 968.10 | 12.15 | 435.22 | 22.07 | 1000.19 | 15.43 | 351.13 | 20.49 | 201.68 | 8.11 |  |  | 222.39 | 12.60 | 0.29 | 0.21 | 0.34 |
| 6 | 7200 | 600 | 969.22 | 13.21 | 435.43 | 20.65 | 1001.33 | 15.44 | 352.12 | 18.71 | 201.49 | 7.88 |  |  | 222.70 | 12.50 | 0.35 | 0.21 | 0.41 |
| 7 | 0 | 600 | 969.76 | 9.89 | 436.81 | 13.96 | 1001.92 | 11.12 | 352.29 | 14.38 | 201.73 | 4.65 | 210.68 | 10.55 | 223.29 | 7.61 | 0.00 | 0.00 | 0.00 |
| 7 | 10 | 600 | 970.74 | 10.13 | 436.37 | 13.76 | 1003.05 | 10.95 | 353.39 | 13.73 | 201.90 | 4.33 | 211.17 | 11.55 | 223.46 | 7.71 | 0.02 | 0.02 | 0.06 |
| 7 | 30 | 600 | 971.09 | 10.04 | 436.06 | 13.90 | 1003.33 | 10.99 | 353.82 | 13.39 | 201.96 | 4.69 | 211.00 | 11.01 | 223.37 | 7.93 | 0.01 | 0.01 | 0.09 |
| 7 | 90 | 600 | 971.24 | 9.32 | 435.54 | 13.05 | 1002.98 | 9.78 | 353.70 | 11.27 | 201.66 | 4.00 | 211.49 | 11.08 | 223.32 | 7.34 | 0.10 | 0.15 | 0.29 |
| 7 | 300 | 600 | 971.59 | 8.50 | 436.12 | 12.67 | 1003.74 | 9.11 | 354.52 | 10.61 | 201.76 | 3.78 | 211.36 | 10.70 | 223.43 | 7.01 | 0.14 | 0.22 | 0.35 |
| 7 | 7200 | 600 | 972.07 | 8.62 | 435.96 | 12.45 | 1004.11 | 8.92 | 354.51 | 10.04 | 201.75 | 3.73 | 211.66 | 10.17 |  | 6.85 | 0.17 | 0.24 | 0.40 |
| 8 | 0 | 600 | 967.78 | 12.05 | 435.81 | 17.10 | 999.68 | 13.85 | 349.96 | 18.64 | 201.45 | 6.25 | 209.74 | 14.33 | 222.84 | 9.10 | 0.00 | 0.00 | 0.00 |
| 8 | 10 | 600 | 970.04 | 11.10 | 436.28 | 15.27 | 1002.33 | 11.95 | 353.02 | 15.29 | 201.93 | 4.70 | 210.78 | 12.93 | 223.45 | 7.95 | 0.15 | 0.16 | 0.22 |
| 8 | 30 | 600 | 971.54 | 9.34 | 436.28 | 13.11 | 1003.81 | 9.87 | 354.01 | 11.78 | 201.85 | 4.12 | 211.49 | 10.56 | 223.50 | 7.11 | 0.33 | 0.33 | 0.46 |
| 8 | 90 | 600 | 971.17 | 9.25 | 435.76 | 13.71 | 1003.50 | 10.22 | 353.74 | 12.03 | 201.65 | 4.31 | 211.41 | 13.13 | 223.38 | 7.80 | 0.28 | 0.30 | 0.44 |
| 8 | 300 | 600 | 971.36 | 8.82 | 436.20 | 12.58 | 1003.77 | 9.68 | 354.36 | 11.35 | 201.78 | 3.96 | 211.14 | 11.27 | 223.33 | 7.49 | 0.37 | 0.35 | 0.48 |
| 8 | 1440 | 600 | 971.11 | 8.27 | 435.47 | 13.45 | 1003.15 | 9.65 | 354.22 | 10.86 | 201.88 | 3.80 | 211.41 | 11.37 | 223.39 | 7.35 | 0.30 | 0.35 | 0.52 |
| 8 | 7200 | 600 | 971.91 | 9.17 | 435.98 | 12.77 | 1004.01 | 9.67 | 354.75 | 10.84 | 201.81 | 3.89 | 211.39 | 11.12 | 223.42 | 7.26 | 0.36 | 0.35 | 0.52 |
| 9 | 0 | 600 | 968.98 | 10.21 | 436.83 | 15.06 | 1001.24 | 11.37 | 351.01 | 16.21 | 201.73 | 5.61 | 210.50 | 9.63 | 222.96 | 8.68 | 0.00 | 0.00 | 0.00 |
| 9 | 10 | 600 | 970.58 | 8.32 | 436.47 | 13.24 | 1003.03 | 9.95 | 353.31 | 12.25 | 201.95 | 4.12 | 211.41 | 11.17 | 223.53 | 7.41 | 0.18 | 0.15 | 0.31 |
| 9 | 30 | 600 | 970.84 | 8.66 | 436.33 | 13.52 | 1003.19 | 9.65 | 353.59 | 11.81 | 201.99 | 4.72 | 210.78 | 9.20 | 223.23 | 7.83 | 0.15 | 0.18 | 0.35 |
| 9 | 90 | 600 | 971.54 | 9.10 | 436.04 | 13.02 | 1003.94 | 9.58 | 354.04 | 11.26 | 201.76 | 3.94 | 211.66 | 12.49 | 223.47 | 7.20 | 0.20 | 0.19 | 0.39 |
| 10 | 0 | 600 | 968.39 | 11.34 | 436.46 | 14.78 | 1000.39 | 12.37 | 350.65 | 16.50 | 201.29 | 9.08 | 210.17 | 10.31 | 222.82 | 9.49 | 0.00 | 0.00 | 0.00 |
| 10 | 10 | 600 | 970.36 | 8.91 | 436.23 | 14.01 | 1002.69 | 10.07 | 352.63 | 13.33 | 201.91 | 4.39 | 211.24 | 11.36 | 223.44 | 8.03 | 0.08 | 0.22 | 0.25 |
| 10 | 30 | 600 | 972.30 | 7.23 | 436.94 | 11.56 | 1004.91 | 8.05 | 354.76 | 9.68 | 201.90 | 3.55 | 211.84 | 8.60 | 223.72 | 6.38 | 0.33 | 0.41 | 0.53 |
| 10 | 90 | 600 | 972.14 | 8.03 | 436.39 | 11.64 | 1004.71 | 8.86 | 354.65 | 10.45 | 201.74 | 3.64 | 211.66 | 11.37 | 223.49 | 6.35 | 0.32 | 0.34 | 0.47 |
| 10 | 300 | 600 | 971.97 | 7.67 | 436.58 | 11.75 | 1004.65 | 8.62 | 354.72 | 9.89 | 201.89 | 3.56 | 211.72 | 10.16 | 223.58 | 6.67 | 0.31 | 0.36 | 0.51 |
| 10 | 1440 | 600 | 972.59 | 6.49 | 436.99 | 10.22 | 1005.22 | 7.22 | 355.30 | 8.37 | 201.83 | 2.83 | 212.30 | 8.67 | 223.82 | 5.61 | 0.47 | 0.49 | 0.63 |
| 10 | 7200 | 600 | 972.53 | 6.29 | 436.91 | 10.22 | 1005.05 | 7.18 | 355.25 | 8.60 | 201.88 | 2.96 | 212.04 | 7.84 | 223.80 | 5.73 | 0.47 | 0.50 | 0.61 |
| 11 | 0 | 600 | 969.51 | 17.19 | 436.96 | 16.79 | 1001.05 | 14.27 | 351.18 | 19.50 | 201.98 | 6.35 | 210.33 | 11.95 | 223.34 | 9.37 | 0.00 | 0.00 | 0.00 |
| 11 | 10 | 600 | 970.53 | 12.79 | 436.57 | 14.97 | 1002.68 | 12.80 | 353.10 | 15.92 | 201.81 | 5.55 | 211.09 | 11.99 | 223.44 | 8.25 | 0.15 | 0.12 | 0.23 |
| 11 | 30 | 600 | 970.88 | 10.27 | 436.15 |  | 1003.23 | 11.17 | 353.50 | 14.32 | 201.74 | 5.01 | 211.00 | 11.48 | 223.31 | 8.12 | 1.42 | 0.25 | 0.33 |
| 11 | 90 | 600 | 971.33 | 11.41 | 436.32 | 13.81 | 1003.63 | 11.68 | 354.24 | 13.78 | 201.95 | 4.65 | 211.37 | 12.50 | 223.63 | 7.58 | 0.25 | 0.21 | 0.36 |
| 11 | 300 | 600 | 971.48 | 10.15 | 436.15 | 13.01 | 1003.86 | 10.49 | 354.20 | 12.71 | 201.78 | 4.05 | 211.04 | 11.97 | 223.32 | 7.41 | 0.32 | 0.31 | 0.43 |
| 11 | 1440 | 600 | 971.51 | 10.64 | 436.29 | 13.06 | 1003.84 | 10.93 | 354.38 | 13.15 | 201.82 | 4.75 | 211.49 | 11.86 | 223.49 | 7.71 | 0.32 | 0.27 | 0.40 |
| 11 | 7200 | 600 | 972.16 | 8.19 | 436.54 | 12.44 | 1004.69 | 9.04 | 354.99 | 10.65 | 201.87 | 4.21 | 211.54 | 9.17 | 223.56 | 6.82 | 0.37 | 0.42 | 0.56 |
| 12 | 0 | 600 | 968.44 | 11.03 | 436.82 | 15.99 | 1000.84 | 13.06 | 350.86 | 18.30 | 201.90 | 6.82 | 210.39 | 10.22 | 222.91 | 9.36 | 0.00 | 0.00 | 0.00 |
| 12 | 10 | 600 | 969.98 | 11.70 | 436.42 | 14.01 | 1002.36 | 12.70 | 352.94 | 15.99 | 201.85 | 5.13 | 210.79 | 11.18 | 223.31 | 8.22 | 0.18 | 0.03 | 0.16 |
| 12 | 30 | 600 | 971.29 | 10.80 | 436.14 | 13.55 | 1003.40 | 11.58 | 353.74 | 14.27 | 201.69 | 5.59 | 211.36 | 11.18 | 223.35 | 8.18 | 0.22 | 0.13 | 0.27 |
| 12 | 90 | 600 | 970.96 | 10.20 | 436.23 | 12.84 | 1003.52 | 10.90 | 353.90 | 12.94 | 201.93 | 4.95 | 211.20 | 9.43 | 223.47 | 7.79 | 0.29 | 0.19 | 0.36 |
| 12 | 300 | 600 | 971.72 | 8.05 | 436.49 | 11.95 | 1004.03 | 8.98 | 354.61 | 10.88 | 201.85 | 3.64 | 211.56 | 9.89 | 223.59 | 6.63 | 0.37 | 0.37 | 0.50 |
| 13 | 0 | 600 | 970.08 | 7.29 | 436.94 | 11.14 | 1002.35 | 9.07 | 352.50 | 12.86 | 201.63 | 3.96 | 210.92 | 7.83 | 223.41 | 6.74 | 0.00 | 0.00 | 0.00 |
| 13 | 10 | 600 | 971.82 | 6.84 | 437.16 | 10.61 | 1004.49 | 7.86 | 354.30 | 9.73 | 201.90 | 3.36 | 211.89 | 8.49 | 223.87 | 5.97 | 0.09 | 0.17 | 0.34 |
| 13 | 30 | 600 | 972.95 | 5.92 | 437.34 | 9.79 | 1005.73 | 6.83 | 355.15 | 7.99 | 201.93 | 2.64 | 212.47 | 7.54 | 224.01 | 5.20 | 0.22 | 0.31 | 0.53 |
| 13 | 90 | 600 | 972.81 | 5.59 | 437.04 | 9.27 | 1005.44 | 6.40 | 354.97 | 7.94 | 201.75 | 2.47 | 212.35 | 6.92 | 223.86 | 5.20 | 0.30 | 0.37 | 0.53 |
| 13 | 300 | 600 | 972.73 | 5.31 | 437.22 | 8.94 | 1005.43 | 6.08 | 355.18 | 7.60 | 201.83 | 2.43 | 212.51 | 6.20 | 223.98 | 4.89 | 0.36 | 0.42 | 0.57 |
| 13 | 1440 | 600 | 972.99 | 5.27 | 437.39 | 8.96 | 1005.79 | 5.98 | 355.40 | 7.47 | 201.91 | 2.30 | 212.68 | 6.47 | 224.08 | 4.89 | 0.36 | 0.43 | 0.58 |
| 14 | 0 | 600 | 970.54 | 7.40 | 437.22 | 10.21 | 1003.17 | 8.08 | 352.64 | 10.94 | 201.72 | 3.07 | 211.62 | 6.99 | 223.76 | 5.75 | 0.00 | 0.00 | 0.00 |
| 14 | 10 | 600 | 971.97 | 6.00 | 437.16 | 10.55 | 1004.55 | 6.59 | 354.43 | 8.65 | 202.02 | 2.47 | 212.48 | 6.47 | 224.08 | 5.42 | -0.07 | 0.24 | 0.31 |
| 14 | 30 | 600 | 972.66 | 5.71 | 437.23 | 9.80 | 1005.39 | 6.73 | 354.95 | 7.97 | 201.94 | 2.72 | 212.41 | 7.35 | 223.95 | 5.26 | 0.08 | 0.22 | 0.40 |
| 14 | 90 | 600 | 972.61 | 5.80 | 437.06 | 9.50 | 1005.38 | 6.53 | 354.99 | 7.91 | 201.74 | 2.67 | 212.24 | 6.70 | 223.82 | 5.26 | 0.14 | 0.25 | 0.41 |
| 14 | 300 | 600 | 972.82 | 5.23 | 437.40 | 9.09 | 1005.63 | 5.99 | 355.33 | 7.26 | 201.85 | 2.40 | 212.48 | 5.92 | 223.97 | 4.91 | 0.21 | 0.34 | 0.50 |
| 14 | 1440 | 600 | 972.62 | 5.63 | 437.22 | 9.44 | 1005.41 | 6.47 | 355.30 | 7.61 | 201.86 | 2.57 | 212.38 | 6.53 | 223.94 | 5.19 | 0.15 | 0.26 | 0.45 |
| 14 | 7200 | 600 | 973.14 | 4.56 | 437.36 | 8.47 | 1005.87 | 5.14 | 355.35 | 6.73 | 201.79 | 2.00 | 212.87 | 5.43 | 224.11 | 4.49 | 0.33 | 0.48 | 0.57 |
| 15 | 0 | 600 | 972.54 | 4.97 | 437.34 | 8.24 | 1005.22 | 5.47 | 353.69 | 8.53 | 201.60 | 2.16 | 212.71 | 4.88 | 223.87 | 4.86 | 0.00 | 0.00 | 0.00 |
| 15 | 10 | 600 | 972.78 | 4.50 | 437.27 | 8.07 | 1005.13 | 4.97 | 354.95 | 7.51 | 201.92 | 2.01 | 212.94 | 4.76 | 224.27 | 4.50 | 0.05 | 0.14 | 0.21 |
| 15 | 30 | 600 | 973.18 | 4.05 | 437.56 | 7.53 | 1006.02 | 4.64 | 355.09 | 6.40 | 201.79 | 1.67 | 213.13 | 4.68 | 224.27 | 4.07 | 0.22 | 0.23 | 0.43 |
| 15 | 90 | 600 | 973.07 | 4.46 | 437.26 | 8.09 | 1005.65 | 5.12 | 355.04 | 6.60 | 201.67 | 1.82 | 212.70 | 5.26 | 224.06 | 4.29 | 0.05 | 0.10 | 0.39 |
| 15 | 300 | 600 | 972.96 | 4.75 | 437.35 | 7.95 | 1005.55 | 5.37 | 355.64 | 6.74 | 201.82 | 2.09 | 212.70 | 4.92 | 224.10 | 4.29 | 0.09 | 0.03 | 0.36 |
| 15 | 7200 | 600 | 973.02 | 3.99 | 437.36 | 7.68 | 1005.75 | 4.60 | 355.37 | 6.70 | 201.80 | 2.08 | 212.90 | 4.62 | 224.12 | 4.25 | 0.17 | 0.24 | 0.37 |
| 16 | 0 | 600 | 971.88 | 5.41 | 437.20 | 8.89 | 1004.49 | 6.08 | 353.46 | 8.70 | 201.63 | 2.40 | 212.39 | 6.04 | 223.86 | 5.12 | 0.00 | 0.00 | 0.00 |
| 16 | 10 | 600 | 972.91 | 5.06 | 437.55 | 8.34 | 1005.57 | 5.76 | 355.04 | 7.79 | 201.89 | 2.13 | 212.86 | 5.09 | 224.18 | 4.57 | 0.14 | 0.08 | 0.18 |
| 16 | 30 | 600 | 973.04 | 4.08 | 437.51 | 7.57 | 1005.92 | 4.74 | 355.16 | 6.43 | 201.78 | 1.73 | 212.96 | 4.51 | 224.17 | 4.06 | 0.34 | 0.32 | 0.45 |
| 16 | 90 | 600 | 973.39 | 4.20 | 437.51 | 7.90 | 1006.19 | 4.89 | 355.19 | 6.90 | 201.76 | 1.98 | 213.05 | 5.01 | 224.16 | 4.33 | 0.25 | 0.28 | 0.35 |
| 16 | 1440 | 600 | 973.27 | 3.77 | 437.64 | 7.41 | 1006.12 | 4.38 | 355.43 | 6.05 | 201.87 | 1.67 | 213.20 | 4.40 | 224.32 | 3.91 | 0.38 | 0.41 | 0.52 |
| 16 | 7200 | 600 | 973.22 | 4.10 | 437.52 | 7.62 | 1005.96 | 4.89 | 355.44 | 6.13 | 201.84 | 1.88 | 212.97 | 5.00 | 224.24 | 3.99 | 0.33 | 0.28 | 0.50 |
| 17 | 0 | 700 | 966.19 | 12.29 | 436.49 | 19.47 | 998.71 | 14.83 | 349.01 | 23.68 | 201.97 | 7.47 | 209.33 | 11.85 | 222.69 | 12.03 | 0.00 | 0.00 | 0.00 |
| 17 | 10 | 700 | 970.04 | 10.15 | 435.14 | 14.08 | 1002.26 | 11.57 | 353.34 | 14.30 | 201.60 | 4.10 |  |  | 223.20 | 8.36 | 0.37 | 0.25 | 0.47 |
| 17 | 30 | 700 | 971.24 | 7.90 | 435.13 | 13.46 | 1003.56 | 9.84 | 354.08 | 10.78 | 201.73 | 4.19 | 211.27 | 13.61 | 223.18 | 7.78 | 0.42 | 0.39 | 0.64 |
| 17 | 90 | 700 | 971.76 | 8.82 | 435.81 | 12.07 | 1004.10 | 9.17 | 354.65 | 10.30 | 201.87 | 3.96 | 211.19 | 11.59 | 223.37 | 7.38 | 0.51 | 0.44 | 0.67 |
| 17 | 300 | 700 | 971.77 | 9.77 | 435.55 | 13.45 | 1004.10 | 10.08 | 354.86 | 10.98 | 201.88 | 4.46 | 210.78 | 11.79 | 223.21 | 8.04 | 0.42 | 0.37 | 0.63 |
| 17 | 1440 | 700 | 971.68 | 9.40 | 435.33 | 12.33 | 1003.97 | 9.87 | 354.68 | 10.07 | 201.68 | 5.44 | 210.84 | 9.90 | 223.14 | 8.34 | 0.49 | 0.38 | 0.68 |
| 17 | 7200 | 700 | 972.03 | 8.29 | 436.14 | 12.15 | 1004.45 | 9.20 | 354.75 | 10.06 | 201.93 | 3.93 | 211.92 | 10.43 | 223.63 | 7.54 | 0.51 | 0.44 | 0.68 |
| 18 | 0 | 700 | 967.23 | 10.32 | 436.59 | 17.47 | 999.47 | 13.48 | 350.34 | 20.59 | 201.72 | 6.87 | 208.95 | 11.99 | 222.87 | 10.98 | 0.00 | 0.00 | 0.00 |
| 18 | 10 | 700 | 970.04 | 10.49 | 435.27 | 13.97 | 1002.40 | 12.10 | 353.67 | 14.79 | 201.63 | 7.15 | 210.46 | 10.70 | 222.84 | 9.12 | 0.28 | 0.12 | 0.34 |
| 18 | 30 | 700 | 971.13 | 9.88 | 434.85 | 13.49 | 1003.31 | 10.92 | 354.37 | 11.54 | 201.60 | 4.49 | 211.01 | 16.65 | 223.05 | 7.73 | 0.32 | 0.22 | 0.53 |
| 18 | 90 | 700 | 971.57 | 9.10 | 435.66 | 11.86 | 1003.92 | 10.12 | 354.82 | 10.93 | 201.79 | 4.25 | 210.80 | 10.66 | 223.22 | 7.70 | 0.45 | 0.29 | 0.57 |
| 18 | 300 | 700 | 971.49 | 9.14 | 435.59 | 12.18 | 1003.85 | 10.14 | 354.70 | 11.39 | 201.78 | 4.56 | 210.85 | 10.86 | 223.20 | 7.97 | 0.42 | 0.29 | 0.54 |
| 18 | 1440 | 700 | 971.63 | 8.77 | 435.71 | 11.64 | 1004.08 | 9.97 | 354.53 | 10.27 | 201.65 | 3.85 | 211.05 | 11.61 | 223.30 | 7.47 | 0.47 | 0.30 | 0.61 |
| 18 | 7200 | 700 | 971.87 | 8.79 | 435.76 | 12.74 | 1004.04 | 9.60 | 354.61 | 10.19 | 201.94 | 4.00 | 211.73 | 12.26 | 223.52 | 7.71 | 0.38 | 0.34 | 0.61 |
| 19 | 0 | 700 | 971.19 | 6.63 | 437.69 | 11.09 | 1003.76 | 7.75 | 353.18 | 11.29 | 201.91 | 3.41 | 211.92 | 8.28 | 223.72 | 6.47 | 0.00 | 0.00 | 0.00 |
| 19 | 10 | 700 | 972.85 | 5.67 | 437.44 | 9.92 | 1005.75 | 6.37 | 355.38 | 7.74 | 201.86 | 2.69 |  |  | 223.94 | 5.12 | 0.19 | 0.24 | 0.46 |
| 19 | 30 | 700 | 973.03 | 4.76 | 437.30 | 9.53 | 1005.75 | 5.94 | 355.28 | 7.26 | 201.78 | 2.47 | 212.66 | 6.95 | 223.91 | 5.13 | 0.26 | 0.31 | 0.52 |
| 19 | 90 | 700 | 972.42 | 5.75 | 437.03 | 10.37 | 1004.92 | 6.67 | 355.00 | 7.70 | 201.80 | 2.74 | 212.66 | 8.28 | 223.86 | 5.69 | 0.12 | 0.18 | 0.47 |
| 19 | 300 | 700 | 972.87 | 5.44 | 437.38 | 9.98 | 1005.59 | 6.38 | 355.46 | 7.59 | 201.93 | 2.58 | 212.47 | 7.43 | 224.03 | 5.52 | 0.18 | 0.23 | 0.48 |
| 19 | 1440 | 700 | 972.87 | 5.30 | 437.25 | 9.67 | 1005.58 | 6.16 | 355.35 | 7.43 | 201.85 | 2.73 | 212.43 | 6.98 | 223.96 | 5.30 | 0.23 | 0.27 | 0.50 |
| 19 | 7200 | 700 | 973.28 | 5.28 | 437.52 | 9.28 | 1006.05 | 6.32 | 355.71 | 7.24 | 201.94 | 2.64 | 212.62 | 6.85 | 224.17 | 5.18 | 0.30 | 0.24 | 0.53 |
| 20 | 0 | 700 | 970.96 | 5.52 | 437.76 | 10.46 | 1003.53 | 7.35 | 353.37 | 9.88 | 201.99 | 3.23 | 211.91 | 7.17 | 223.93 | 6.05 | 0.00 | 0.00 | 0.00 |
| 20 | 10 | 700 | 972.69 | 5.41 | 437.55 | 9.78 | 1005.63 | 6.58 | 355.17 | 7.77 | 201.77 | 2.82 | 212.41 | 7.57 | 223.91 | 5.28 | 0.12 | 0.14 | 0.34 |
| 20 | 30 | 700 | 973.05 | 5.76 | 436.98 | 10.33 | 1005.72 | 6.65 | 355.45 | 7.65 | 201.73 | 2.71 | 213.03 | 11.14 | 223.78 | 5.47 | 0.02 | 0.13 | 0.36 |
| 20 | 90 | 700 | 972.71 | 5.40 | 437.17 | 10.23 | 1005.36 | 6.78 | 355.19 | 8.01 | 201.68 | 2.88 | 212.59 | 8.04 | 223.74 | 5.78 | 0.04 | 0.10 | 0.30 |
| 20 | 300 | 700 | 972.75 | 4.95 | 437.30 | 9.47 | 1005.45 | 5.64 | 355.34 | 7.09 | 201.97 | 2.29 | 213.01 | 8.31 | 224.14 | 5.09 | 0.18 | 0.31 | 0.44 |
| 20 | 1440 | 700 | 973.03 | 4.85 | 437.35 | 9.10 | 1005.89 | 5.68 | 355.45 | 6.81 | 201.80 | 2.24 | 212.75 | 6.66 | 224.03 | 4.90 | 0.25 | 0.31 | 0.49 |
| 20 | 7200 | 700 | 973.41 | 5.07 | 437.57 | 9.11 | 1006.38 | 5.39 | 355.75 | 6.61 | 202.08 | 2.24 | 213.44 | 8.40 | 224.28 | 4.89 | 0.25 | 0.36 | 0.52 |
| 21 | 0 | 700 | 970.88 | 9.47 | 437.24 | 11.98 | 1003.09 | 9.36 | 353.00 | 12.15 | 201.83 | 4.35 | 211.74 | 7.37 | 223.73 | 6.37 | 0.00 | 0.00 | 0.00 |
| 21 | 10 | 700 | 972.11 | 8.87 | 436.79 | 11.42 | 1004.74 | 9.69 | 354.73 | 9.98 | 201.85 | 3.33 | 211.96 | 9.47 | 223.83 | 5.89 | 0.08 | -0.04 | 0.25 |
| 21 | 30 | 700 | 973.07 | 6.14 | 436.95 | 9.81 | 1005.74 | 6.78 | 355.25 | 7.86 | 201.80 | 2.72 | 212.51 | 7.69 | 223.87 | 5.39 | 0.31 | 0.35 | 0.50 |
| 21 | 90 | 700 | 972.77 | 6.92 | 436.73 | 10.23 | 1005.26 | 7.50 | 355.20 | 8.54 | 201.87 | 2.88 | 212.19 | 8.41 | 223.93 | 5.83 | 0.25 | 0.25 | 0.42 |
| 21 | 1440 | 700 | 973.01 | 5.50 | 437.05 | 9.07 | 1005.64 | 6.00 | 355.32 | 7.43 | 201.86 | 2.34 | 212.77 | 7.00 | 224.06 | 5.03 | 0.42 | 0.45 | 0.55 |
| 22 | 0 | 700 | 968.87 | 8.59 | 436.73 | 14.00 | 1001.15 | 10.92 | 351.61 | 16.19 | 201.80 | 5.37 | 210.22 | 9.23 | 222.97 | 8.78 | 0.00 | 0.00 | 0.00 |
| 22 | 10 | 700 | 972.12 | 7.86 | 436.68 | 11.59 | 1004.75 | 8.56 | 354.81 | 9.80 | 201.87 | 3.50 | 211.60 | 8.90 | 223.67 | 6.58 | 0.27 | 0.26 | 0.51 |
| 22 | 30 | 700 | 972.84 | 6.51 | 436.87 | 10.60 | 1005.38 | 7.29 | 355.24 | 8.27 | 201.72 | 3.23 | 211.96 | 8.19 | 223.68 | 5.82 | 0.38 | 0.40 | 0.63 |
| 22 | 90 | 700 | 972.20 | 6.49 | 436.52 | 10.80 | 1004.69 | 7.96 | 354.92 | 8.70 | 201.80 | 3.04 | 212.30 | 10.35 | 223.67 | 5.94 | 0.36 | 0.33 | 0.59 |
| 22 | 300 | 700 | 972.09 | 6.90 | 436.26 | 10.88 | 1004.43 | 7.86 | 354.94 | 8.53 | 201.80 | 2.93 | 211.70 | 8.39 | 223.68 | 6.22 | 0.35 | 0.34 | 0.61 |
| 22 | 1440 | 700 | 972.44 | 6.12 | 436.83 | 9.42 | 1005.32 | 7.72 | 355.01 | 8.14 | 201.68 | 3.10 | 211.95 | 7.10 | 223.73 | 5.69 | 0.51 | 0.35 | 0.64 |
| 22 | 7200 | 700 | 972.43 | 6.04 | 436.73 | 9.50 | 1004.98 | 7.29 | 355.23 | 7.83 | 201.97 | 2.80 | 212.08 | 6.93 | 224.00 | 5.55 | 0.50 | 0.40 | 0.66 |
| 23 | 0 | 700 | 969.21 | 8.58 | 436.89 | 13.48 | 1001.51 | 10.49 | 352.16 | 15.79 | 201.84 | 5.17 | 210.25 | 9.56 | 223.12 | 8.25 | 0.00 | 0.00 | 0.00 |
| 23 | 10 | 700 | 971.69 | 7.60 | 436.50 | 11.54 | 1004.35 | 8.84 | 354.73 | 10.45 | 201.76 | 3.84 | 211.33 | 8.12 | 223.47 | 6.53 | 0.23 | 0.19 | 0.44 |
| 23 | 30 | 700 | 972.56 | 6.18 | 436.67 | 10.77 | 1005.20 | 7.57 | 355.25 | 8.19 | 201.71 | 2.78 | 212.50 | 11.25 | 223.63 | 5.59 | 0.32 | 0.34 | 0.62 |
| 23 | 90 | 700 | 972.82 | 6.82 | 436.82 | 10.93 | 1005.32 | 8.26 | 355.18 | 8.61 | 201.80 | 2.83 | 212.96 | 13.01 | 223.90 | 5.60 | 0.30 | 0.26 | 0.59 |
| 23 | 300 | 700 | 971.87 | 6.94 | 436.23 | 10.87 | 1004.25 | 8.13 | 354.85 | 8.88 | 201.83 | 3.30 | 211.64 | 8.35 | 223.70 | 6.27 | 0.31 | 0.27 | 0.57 |
| 23 | 1440 | 700 | 972.62 | 6.18 | 436.83 | 9.48 | 1005.36 | 7.21 | 355.21 | 7.75 | 201.81 | 2.95 | 212.09 | 7.30 | 223.89 | 5.58 | 0.47 | 0.38 | 0.66 |
| 23 | 7200 | 700 | 972.46 | 5.96 | 436.69 | 9.56 | 1004.96 | 7.23 | 355.09 | 7.78 | 201.93 | 2.83 | 212.15 | 7.01 | 223.95 | 5.76 | 0.46 | 0.38 | 0.66 |
| 24 | 0 | 800 | 970.12 | 9.32 | 437.08 | 12.92 | 1002.42 | 10.73 | 352.85 | 14.70 | 201.78 | 4.97 | 210.75 | 8.82 | 223.43 | 7.98 | 0.00 | 0.00 | 0.00 |
| 24 | 10 | 800 | 972.95 | 6.45 | 436.99 | 9.58 | 1005.74 | 7.44 | 355.49 | 8.04 | 201.83 | 3.11 | 212.11 | 7.43 | 223.89 | 5.41 | 0.42 | 0.37 | 0.60 |
| 24 | 30 | 800 | 971.96 | 5.22 | 437.17 | 7.61 | 1005.61 | 5.92 | 355.41 | 6.70 | 201.58 | 2.19 | 212.51 | 5.38 | 223.95 | 4.52 | 0.67 | 0.54 | 0.72 |
| 24 | 90 | 800 | 972.86 | 5.57 | 437.05 | 8.77 | 1005.76 | 6.73 | 355.19 | 7.40 | 201.66 | 2.60 | 212.30 | 6.30 | 223.87 | 5.08 | 0.52 | 0.45 | 0.66 |
| 24 | 300 | 800 | 973.26 | 4.30 | 437.58 | 7.24 | 1006.28 | 5.83 | 355.28 | 6.37 | 201.80 | 2.09 | 212.81 | 5.06 | 224.13 | 4.39 | 0.72 | 0.55 | 0.75 |
| 24 | 1440 | 800 | 973.28 | 3.85 | 437.76 | 7.32 | 1006.15 | 5.21 | 355.49 | 6.24 | 201.88 | 1.90 | 213.11 | 4.55 | 224.38 | 4.21 | 0.71 | 0.63 | 0.76 |
| 24 | 7200 | 800 | 972.99 | 3.60 | 437.54 | 7.44 | 1005.58 | 4.73 | 355.03 | 6.40 | 201.79 | 1.82 | 212.99 | 4.20 | 224.32 | 4.29 | 0.69 | 0.68 | 0.75 |
| 25 | 0 | 800 | 970.14 | 8.18 | 437.46 | 12.68 | 1002.73 | 9.91 | 352.46 | 14.93 | 201.78 | 4.98 | 210.98 | 8.49 | 223.30 | 7.65 | 0.00 | 0.00 | 0.00 |
| 25 | 10 | 800 | 972.73 | 5.82 | 437.13 | 9.31 | 1005.64 | 6.81 | 355.33 | 7.88 | 201.87 | 2.85 | 212.19 | 6.51 | 223.94 | 5.20 | 0.44 | 0.39 | 0.62 |
| 25 | 30 | 800 | 972.86 | 5.28 | 436.99 | 8.47 | 1005.71 | 6.66 | 355.35 | 7.20 | 201.64 | 2.52 | 212.21 | 6.20 | 223.82 | 4.88 | 0.55 | 0.41 | 0.68 |
| 25 | 90 | 800 | 972.78 | 4.82 | 437.12 | 7.69 | 1005.73 | 6.37 | 354.98 | 6.91 | 201.56 | 2.28 | 212.39 | 5.85 | 223.81 | 4.84 | 0.65 | 0.44 | 0.71 |
| 25 | 300 | 800 | 973.47 | 4.42 | 437.66 | 7.33 | 1006.54 | 5.85 | 355.59 | 6.36 | 201.83 | 2.02 | 212.92 | 5.05 | 224.23 | 4.26 | 0.70 | 0.51 | 0.76 |
| 25 | 1440 | 800 | 973.23 | 3.81 | 437.78 | 7.24 | 1006.19 | 5.07 | 355.35 | 6.20 | 201.81 | 1.94 | 213.04 | 4.54 | 224.29 | 4.19 | 0.71 | 0.60 | 0.77 |
| 25 | 7200 | 800 | 973.37 | 3.35 | 437.89 | 6.96 | 1006.33 | 4.45 | 355.45 | 5.82 | 201.77 | 1.77 | 213.13 | 4.04 | 224.32 | 3.99 | 0.74 | 0.68 | 0.80 |
| 26 | 0 | 800 | 971.33 | 7.63 | 437.34 | 11.40 | 1003.54 | 8.66 | 353.30 | 11.45 | 201.86 | 3.73 | 211.89 | 8.05 | 223.80 | 6.27 | 0.00 | 0.00 | 0.00 |
| 26 | 10 | 800 | 972.36 | 5.01 | 436.65 | 9.70 | 1004.67 | 5.49 | 354.61 | 7.35 | 201.79 | 2.16 | 212.59 | 6.29 | 223.96 | 5.21 | 0.27 | 0.47 | 0.52 |
| 26 | 90 | 800 | 972.84 | 4.71 | 437.13 | 8.48 | 1005.75 | 5.71 | 355.01 | 6.75 | 201.66 | 2.19 | 212.68 | 5.92 | 223.98 | 4.66 | 0.46 | 0.44 | 0.60 |
| 26 | 300 | 800 | 973.49 | 3.68 | 437.93 | 7.15 | 1006.56 | 5.10 | 355.45 | 6.06 | 201.88 | 1.84 | 213.31 | 4.31 | 224.40 | 3.98 | 0.66 | 0.53 | 0.69 |
| 26 | 1440 | 800 | 972.92 | 3.85 | 437.60 | 7.42 | 1005.81 | 5.32 | 354.88 | 6.53 | 201.71 | 1.86 | 213.03 | 4.57 | 224.21 | 4.23 | 0.62 | 0.49 | 0.63 |
| 26 | 7200 | 800 | 973.01 | 3.98 | 437.74 | 7.31 | 1006.43 | 5.29 | 355.01 | 6.36 | 201.82 | 1.88 | 213.39 | 4.90 | 224.34 | 4.17 | 0.64 | 0.50 | 0.65 |
| 27 | 0 | 800 | 970.62 | 7.88 | 437.23 | 12.18 | 1003.57 | 8.55 | 353.50 | 12.73 | 201.69 | 3.72 | 211.81 | 9.44 | 223.50 | 6.42 | 0.00 | 0.00 | 0.00 |
| 27 | 10 | 800 | 972.94 | 5.45 | 437.25 | 9.01 | 1006.05 | 6.62 | 355.35 | 7.39 | 201.80 | 2.53 | 212.68 | 6.72 | 223.99 | 5.05 | 0.44 | 0.29 | 0.58 |
| 27 | 30 | 800 | 972.88 | 5.01 | 437.19 | 8.89 | 1005.64 | 6.16 | 355.00 | 7.11 | 201.69 | 2.21 | 212.65 | 6.15 | 224.00 | 4.84 | 0.46 | 0.36 | 0.62 |
| 27 | 90 | 800 | 972.51 | 5.81 | 436.95 | 9.04 | 1005.87 | 6.47 | 354.83 | 7.43 | 201.56 | 2.41 | 212.84 | 6.87 | 223.89 | 5.13 | 0.44 | 0.31 | 0.58 |
| 27 | 300 | 800 | 973.28 | 4.15 | 437.65 | 7.73 | 1006.27 | 5.47 | 355.24 | 6.40 | 201.82 | 1.93 | 213.14 | 4.97 | 224.29 | 4.32 | 0.62 | 0.46 | 0.69 |
| 27 | 1440 | 800 | 973.00 | 4.86 | 437.37 | 8.47 | 1005.65 | 6.16 | 355.00 | 7.11 | 201.89 | 2.20 | 212.80 | 5.35 | 224.21 | 4.86 | 0.52 | 0.36 | 0.62 |
| 27 | 7200 | 800 | 972.96 | 4.52 | 437.39 | 8.22 | 1005.88 | 5.94 | 354.95 | 6.83 | 201.80 | 2.18 | 212.93 | 5.95 | 224.16 | 4.72 | 0.55 | 0.39 | 0.65 |
| 28 | 0 | 800 | 972.31 | 5.58 | 437.43 | 9.22 | 1004.71 | 6.29 | 354.47 | 8.40 | 201.88 | 2.14 | 212.80 | 6.19 | 224.25 | 4.86 | 0.00 | 0.00 | 0.00 |
| 28 | 10 | 800 | 974.20 | 3.57 | 438.16 | 6.98 | 1007.39 | 3.87 | 356.10 | 5.15 | 201.93 | 1.41 | 213.79 | 3.92 | 224.58 | 3.43 | 0.53 | 0.55 | 0.68 |
| 28 | 30 | 800 | 973.64 | 4.71 | 437.42 | 8.60 | 1006.41 | 4.82 | 355.74 | 6.11 | 201.88 | 1.80 | 213.15 | 5.58 | 224.25 | 4.29 | 0.15 | 0.33 | 0.48 |
| 28 | 90 | 800 | 974.00 | 3.38 | 437.89 | 6.93 | 1007.28 | 3.74 | 355.87 | 5.04 | 201.70 | 1.29 | 213.66 | 3.82 | 224.37 | 3.41 | 0.54 | 0.58 | 0.70 |
| 28 | 300 | 800 | 973.77 | 4.62 | 437.51 | 8.31 | 1006.54 | 4.59 | 355.75 | 5.97 | 201.99 | 1.66 | 213.36 | 5.40 | 224.42 | 4.20 | 0.22 | 0.39 | 0.51 |
| 28 | 1440 | 800 | 974.09 | 3.24 | 438.04 | 6.71 | 1007.26 | 3.51 | 356.03 | 5.01 | 201.85 | 1.25 | 213.75 | 3.67 | 224.53 | 3.34 | 0.59 | 0.63 | 0.71 |
| 29 | 0 | 800 | 971.83 | 5.43 | 437.06 | 9.77 | 1004.15 | 6.89 | 353.97 | 8.26 | 201.88 | 2.11 | 212.58 | 6.08 | 224.02 | 4.95 | 0.00 | 0.00 | 0.00 |
| 29 | 10 | 800 | 973.96 | 3.89 | 437.95 | 7.44 | 1006.92 | 4.17 | 355.93 | 5.51 | 201.99 | 1.57 | 213.56 | 4.29 | 224.51 | 3.72 | 0.49 | 0.55 | 0.59 |
| 29 | 30 | 800 | 973.87 | 3.94 | 437.77 | 7.57 | 1006.84 | 4.24 | 355.82 | 5.55 | 201.84 | 1.49 | 213.44 | 4.41 | 224.37 | 3.81 | 0.46 | 0.53 | 0.58 |
| 29 | 90 | 800 | 973.87 | 3.39 | 437.84 | 6.83 | 1007.21 | 3.66 | 355.87 | 5.11 | 201.70 | 1.30 | 213.61 | 3.82 | 224.33 | 3.43 | 0.62 | 0.65 | 0.68 |
| 29 | 300 | 800 | 974.07 | 3.64 | 437.94 | 7.30 | 1007.04 | 3.88 | 355.93 | 5.40 | 202.04 | 1.46 | 213.67 | 4.30 | 224.59 | 3.76 | 0.52 | 0.60 | 0.61 |
| 29 | 1440 | 800 | 973.85 | 3.05 | 437.99 | 6.55 | 1007.09 | 3.37 | 355.77 | 4.89 | 201.84 | 1.21 | 213.76 | 3.70 | 224.53 | 3.35 | 0.68 | 0.71 | 0.72 |
| 30 | 0 | 800 | 966.60 | 15.36 | 435.37 | 19.72 | 997.89 | 16.05 | 348.99 | 22.37 | 201.28 | 5.66 | 207.18 | 23.08 | 222.88 | 10.29 | 0.00 | 0.00 | 0.00 |
| 30 | 10 | 800 | 970.96 | 9.97 | 435.31 | 13.76 | 1002.45 | 9.88 | 353.39 | 11.14 | 201.71 | 4.11 | 211.05 | 10.50 | 223.23 | 8.01 | 0.40 | 0.44 | 0.60 |
| 30 | 30 | 800 | 971.47 | 7.82 | 435.25 | 12.14 | 1003.14 | 8.27 | 353.99 | 9.49 | 201.54 | 3.35 | 211.28 | 9.45 | 223.23 | 6.99 | 0.51 | 0.55 | 0.69 |
| 30 | 300 | 800 |  |  | 435.55 | 12.57 | 1002.78 | 9.65 | 353.48 | 10.40 | 201.81 | 2.91 | 211.25 | 9.47 | 223.61 | 7.34 | 0.49 | 0.45 | 0.64 |
| 30 | 1440 | 800 | 972.58 | 6.46 | 436.74 | 9.74 | 1005.33 | 7.05 | 355.08 | 7.39 | 201.83 | 3.00 | 211.86 | 7.39 | 223.84 | 5.83 | 0.68 | 0.64 | 0.80 |
| 31 | 0 | 800 | 967.06 | 39.96 | 435.11 | 24.32 | 997.90 | 19.14 | 348.52 | 27.28 | 201.69 | 10.60 | 209.52 | 17.98 | 222.41 | 9.58 | 0.00 | 0.00 | 0.00 |
| 31 | 10 | 800 | 968.51 | 12.81 | 433.34 | 17.00 | 999.18 | 14.89 | 351.87 | 15.19 | 201.56 | 3.80 |  |  | 222.84 | 9.64 | 0.38 | 0.25 | 0.51 |
| 31 | 30 | 800 | 970.52 | 10.90 | 434.40 | 15.12 | 1001.95 | 12.33 | 353.10 | 12.86 | 201.47 | 4.71 |  |  | 223.11 | 8.08 | 0.48 | 0.40 | 0.61 |
| 31 | 90 | 800 | 971.05 | 13.78 | 434.47 | 13.29 | 1001.09 | 9.52 | 353.07 | 11.05 | 201.72 | 3.63 | 211.40 | 9.05 | 223.29 | 7.81 | 0.57 | 0.56 | 0.69 |
| 31 | 300 | 800 | 970.06 | 9.29 | 434.32 | 14.10 | 1000.79 | 10.43 | 352.68 | 12.18 | 201.47 | 4.19 | 210.56 | 12.76 | 222.98 | 8.60 | 0.53 | 0.51 | 0.64 |
| 32 | 0 | 800 | 969.39 | 9.11 | 436.64 | 14.32 | 1001.56 | 10.71 | 352.06 | 14.95 | 201.72 | 4.49 | 210.78 | 12.88 | 223.22 | 7.93 | 0.00 | 0.00 | 0.00 |
| 32 | 10 | 800 | 972.66 | 6.55 | 436.77 | 10.24 | 1005.17 | 7.21 | 355.21 | 8.30 | 201.85 | 3.00 | 212.06 | 7.56 | 223.83 | 5.73 | 0.44 | 0.40 | 0.59 |
| 32 | 30 | 800 | 972.42 | 6.54 | 436.45 | 10.35 | 1004.80 | 7.29 | 354.90 | 8.33 | 201.65 | 2.95 | 211.90 | 8.20 | 223.66 | 5.92 | 0.43 | 0.39 | 0.58 |
| 32 | 90 | 800 | 972.74 | 6.51 | 436.77 | 10.43 | 1005.35 | 7.23 | 355.16 | 8.21 | 201.96 | 2.85 | 212.47 | 8.57 | 224.01 | 5.74 | 0.42 | 0.40 | 0.59 |
| 32 | 300 | 800 | 972.76 | 5.69 | 436.76 | 9.43 | 1005.27 | 6.53 | 355.15 | 7.58 | 201.84 | 2.55 | 212.27 | 6.80 | 223.99 | 5.50 | 0.52 | 0.47 | 0.65 |
| 32 | 1440 | 800 | 973.17 | 6.03 | 437.28 | 8.45 | 1005.91 | 6.42 | 355.34 | 8.23 | 201.80 | 2.43 | 212.87 | 5.76 | 224.23 | 5.24 | 0.63 | 0.49 | 0.59 |
| 33 | 0 | 800 | 969.09 | 9.59 | 436.83 | 14.58 | 1001.16 | 10.67 | 351.34 | 15.31 | 201.95 | 5.50 | 210.68 | 9.48 | 223.21 | 8.40 | 0.00 | 0.00 | 0.00 |
| 33 | 10 | 800 | 972.53 | 6.65 | 436.62 | 10.29 | 1005.00 | 7.63 | 355.07 | 8.58 | 201.76 | 2.75 | 212.56 | 11.37 | 223.81 | 5.66 | 0.45 | 0.35 | 0.57 |
| 33 | 30 | 800 | 972.67 | 6.22 | 436.80 | 10.15 | 1005.31 | 6.92 | 355.24 | 7.96 | 201.66 | 2.71 | 212.21 | 8.25 | 223.72 | 5.63 | 0.46 | 0.43 | 0.63 |
| 33 | 90 | 800 | 972.41 | 6.19 | 436.52 | 10.20 | 1004.72 | 6.93 | 354.91 | 8.26 | 201.95 | 2.79 | 212.36 | 7.88 | 223.96 | 5.85 | 0.46 | 0.43 | 0.60 |
| 33 | 300 | 800 | 972.94 | 5.54 | 437.15 | 9.26 | 1005.78 | 6.38 | 355.44 | 7.51 | 201.77 | 2.83 | 212.24 | 6.59 | 223.90 | 5.39 | 0.56 | 0.49 | 0.67 |
| 33 | 1440 | 800 | 972.84 | 5.32 | 437.32 | 8.65 | 1005.70 | 6.24 | 355.32 | 7.31 | 201.84 | 2.48 | 212.54 | 6.57 | 224.06 | 5.20 | 0.62 | 0.51 | 0.68 |
| 34 | 0 | 800 | 969.17 | 8.43 | 436.84 | 12.22 | 1001.29 | 10.59 | 351.54 | 14.07 | 201.45 | 7.34 | 211.57 | 8.39 | 223.32 | 8.26 | 0.00 | 0.00 | 0.00 |
| 34 | 10 | 800 | 972.44 | 7.78 | 436.31 | 11.53 | 1005.05 | 8.56 | 355.13 | 9.22 | 201.80 | 3.44 | 212.29 | 12.48 | 223.57 | 6.50 | 0.10 | 0.23 | 0.46 |
| 34 | 30 | 800 | 971.69 | 7.67 | 435.63 | 11.72 | 1004.03 | 8.41 | 354.38 | 9.30 | 201.57 | 3.28 |  |  | 223.35 | 6.90 | 0.07 | 0.25 | 0.46 |
| 34 | 90 | 800 | 971.94 | 7.60 | 435.80 | 11.81 | 1003.95 | 8.14 | 354.60 | 8.94 | 201.82 | 3.67 | 211.77 | 9.29 | 223.61 | 7.08 | 0.06 | 0.28 | 0.49 |
| 34 | 300 | 800 | 972.46 | 4.88 | 436.69 | 8.46 | 1004.98 | 6.52 | 354.83 | 7.37 | 201.73 | 2.45 | 212.21 | 6.33 | 223.89 | 4.87 | 0.52 | 0.47 | 0.64 |
| 34 | 7200 | 800 | 971.61 | 3.89 | 436.37 | 8.58 | 1003.28 | 5.17 | 353.62 | 7.20 | 201.58 | 2.01 | 212.32 | 4.74 | 223.97 | 4.98 | 0.50 | 0.62 | 0.66 |
| 35 | 0 | 800 | 968.30 | 10.78 | 436.72 | 16.17 | 1000.49 | 12.52 | 350.65 | 18.43 | 201.83 | 4.82 | 208.92 | 36.31 | 223.13 | 8.71 | 0.00 | 0.00 | 0.00 |
| 35 | 10 | 800 | 971.89 | 7.37 | 435.97 | 11.13 | 1003.88 | 8.12 | 354.59 | 9.06 | 201.68 | 3.64 | 211.50 | 8.68 | 223.46 | 6.67 | 0.45 | 0.41 | 0.63 |
| 35 | 30 | 800 | 971.82 | 7.41 | 435.75 | 11.67 | 1003.90 | 7.92 | 354.44 | 8.79 | 201.59 | 3.83 | 211.88 | 8.47 | 223.39 | 6.79 | 0.40 | 0.43 | 0.65 |
| 35 | 90 | 800 | 972.13 | 7.28 | 436.09 | 11.49 | 1004.31 | 7.92 | 354.65 | 8.75 | 201.87 | 3.50 | 201.87 | 8.91 | 223.73 | 6.59 | 0.42 | 0.43 | 0.65 |
| 35 | 300 | 800 | 972.24 | 7.22 | 436.14 | 10.67 | 1004.59 | 8.05 | 354.70 | 8.74 | 201.77 | 3.14 | 211.93 | 9.69 | 223.65 | 6.43 | 0.49 | 0.42 | 0.65 |
| 35 | 1440 | 800 | 971.31 | 6.24 | 435.71 | 11.44 | 1002.99 | 7.56 | 353.84 | 8.43 | 201.60 | 2.82 | 211.60 | 7.59 | 223.62 | 6.33 | 0.42 | 0.47 | 0.67 |
| 36 | 0 | 900 | 969.73 | 8.60 | 436.88 | 13.36 | 1002.02 | 10.45 | 352.05 | 14.46 | 201.73 | 5.02 | 210.76 | 8.32 | 223.18 | 7.67 | 0.00 | 0.00 | 0.00 |
| 36 | 10 | 900 | 972.30 | 5.81 | 436.57 | 9.20 | 1004.64 | 6.88 | 354.60 | 7.50 | 201.83 | 2.61 | 212.46 | 7.42 | 223.99 | 5.48 | 0.50 | 0.42 | 0.64 |
| 36 | 30 | 900 | 972.53 | 4.99 | 436.69 | 8.22 | 1005.06 | 6.36 | 354.77 | 7.36 | 201.57 | 2.40 | 212.45 | 6.32 | 223.86 | 5.08 | 0.61 | 0.48 | 0.65 |
| 36 | 90 | 900 | 972.51 | 4.81 | 436.72 | 8.16 | 1005.09 | 6.07 | 354.63 | 6.99 | 201.53 | 2.21 | 212.28 | 5.42 | 223.84 | 4.82 | 0.62 | 0.51 | 0.69 |
| 36 | 300 | 900 | 972.75 | 3.80 | 437.30 | 7.14 | 1005.72 | 5.23 | 354.87 | 6.08 | 201.45 | 1.92 | 212.63 | 4.32 | 223.95 | 4.03 | 0.74 | 0.61 | 0.77 |
| 37 | 0 | 900 | 969.57 | 8.28 | 436.83 | 13.04 | 1001.85 | 9.90 | 352.04 | 14.27 | 201.79 | 4.70 | 210.70 | 8.50 | 223.28 | 7.74 | 0.00 | 0.00 | 0.00 |
| 37 | 10 | 900 | 972.60 | 5.85 | 436.73 | 9.24 | 1005.11 | 6.91 | 354.94 | 7.52 | 201.81 | 2.73 | 212.24 | 7.42 | 223.91 | 5.57 | 0.47 | 0.37 | 0.63 |
| 37 | 30 | 900 | 972.63 | 4.76 | 436.85 | 7.82 | 1005.27 | 6.24 | 354.79 | 6.99 | 201.54 | 2.24 | 212.43 | 5.71 | 223.85 | 4.78 | 0.65 | 0.46 | 0.68 |
| 37 | 90 | 900 | 972.93 | 4.71 | 437.02 | 8.10 | 1005.75 | 5.54 | 355.18 | 6.52 | 201.67 | 2.13 | 212.45 | 5.59 | 223.97 | 4.73 | 0.61 | 0.55 | 0.73 |
| 37 | 300 | 900 | 973.38 | 3.92 | 437.63 | 7.36 | 1006.29 | 4.84 | 355.60 | 5.91 | 201.98 | 1.86 | 213.07 | 4.62 | 224.44 | 4.17 | 0.71 | 0.63 | 0.78 |
| 38 | 0 | 900 | 968.22 | 11.77 | 436.67 | 15.43 | 1000.60 | 13.49 | 350.64 | 19.14 | 201.46 | 8.20 | 209.81 | 10.83 | 222.86 | 10.17 | 0.00 | 0.00 | 0.00 |
| 38 | 10 | 900 | 972.68 | 6.17 | 436.97 | 9.32 | 1005.41 | 7.37 | 355.25 | 8.14 | 201.94 | 2.84 | 212.26 | 7.41 | 224.00 | 5.56 | 0.59 | 0.53 | 0.71 |
| 38 | 30 | 900 | 972.31 | 7.39 | 436.24 | 10.46 | 1004.90 | 8.94 | 354.47 | 8.89 | 201.63 | 3.44 | 211.69 | 9.05 | 223.64 | 6.08 | 0.48 | 0.39 | 0.66 |
| 38 | 90 | 900 | 972.49 | 6.70 | 436.55 | 9.97 | 1005.00 | 8.38 | 354.51 | 8.21 | 201.70 | 3.18 | 211.97 | 8.47 | 223.84 | 5.80 | 0.52 | 0.44 | 0.70 |
| 38 | 300 | 900 | 971.50 | 4.73 | 436.27 | 8.85 | 1003.56 | 6.25 | 353.76 | 7.57 | 201.41 | 2.38 | 211.98 | 5.68 | 223.68 | 5.19 | 0.63 | 0.62 | 0.74 |
| 39 | 0 | 900 | 969.03 | 9.47 | 436.63 | 14.49 | 1001.20 | 11.02 | 351.43 | 16.36 | 201.89 | 8.38 | 210.59 | 9.02 | 222.90 | 8.87 | 0.00 | 0.00 | 0.00 |
| 39 | 10 | 900 | 972.45 | 7.05 | 436.54 | 10.43 | 1004.77 | 7.47 | 355.05 | 8.62 | 201.99 | 3.39 | 212.04 | 8.71 | 223.90 | 6.43 | 0.43 | 0.39 | 0.61 |
| 39 | 30 | 900 | 972.23 | 6.72 | 436.04 | 10.53 | 1004.54 | 7.47 | 354.60 | 8.16 | 201.63 | 3.01 | 211.62 | 8.28 | 223.61 | 6.17 | 0.42 | 0.39 | 0.64 |
| 39 | 90 | 900 | 972.23 | 6.32 | 436.15 | 10.03 | 1004.53 | 6.96 | 354.56 | 7.77 | 201.64 | 2.78 | 211.79 | 7.39 | 223.70 | 5.96 | 0.47 | 0.45 | 0.67 |
| 39 | 300 | 900 | 972.10 | 3.41 | 436.89 | 7.43 | 1004.49 | 5.02 | 354.15 | 6.53 | 201.35 | 1.93 | 212.40 | 4.18 | 223.81 | 4.33 | 0.74 | 0.66 | 0.77 |
| 40 | 0 | 900 | 969.08 | 9.22 | 436.63 | 13.74 | 1001.19 | 11.02 | 351.54 | 14.84 | 201.72 | 4.96 | 210.48 | 9.55 | 223.27 | 8.01 | 0.00 | 0.00 | 0.00 |
| 40 | 10 | 900 | 972.13 | 6.81 | 436.37 | 10.22 | 1004.55 | 7.95 | 354.72 | 8.80 | 201.80 | 3.20 | 211.85 | 7.93 | 223.78 | 6.29 | 0.40 | 0.34 | 0.54 |
| 40 | 30 | 900 | 971.92 | 7.12 | 435.97 | 10.64 | 1004.27 | 8.18 | 354.40 | 8.46 | 201.60 | 3.32 | 211.35 | 8.67 | 223.52 | 6.47 | 0.35 | 0.31 | 0.57 |
| 40 | 90 | 900 | 972.37 | 5.87 | 436.46 | 9.02 | 1004.79 | 6.77 | 354.48 | 7.54 | 201.53 | 2.45 | 212.07 | 6.58 | 223.73 | 5.32 | 0.54 | 0.47 | 0.65 |
| 41 | 0 | 900 | 968.04 | 9.90 | 436.51 | 15.30 | 1000.22 | 11.83 | 350.39 | 17.55 | 201.91 | 7.16 | 210.37 | 9.89 | 223.01 | 9.99 | 0.00 | 0.00 | 0.00 |
| 41 | 10 | 900 | 972.33 | 7.34 | 436.24 | 10.98 | 1004.66 | 7.93 | 354.97 | 8.76 | 201.81 | 3.26 | 211.61 | 8.89 | 223.63 | 6.29 | 0.42 | 0.39 | 0.63 |
| 41 | 30 | 900 | 972.35 | 6.81 | 436.27 | 9.99 | 1004.93 | 7.81 | 354.68 | 7.95 | 201.65 | 3.04 | 211.69 | 7.95 | 223.61 | 6.09 | 0.52 | 0.40 | 0.69 |
| 41 | 90 | 900 | 972.50 | 5.92 | 436.62 | 8.71 | 1005.18 | 7.43 | 354.75 | 7.95 | 201.58 | 2.70 | 212.01 | 7.26 | 223.73 | 5.43 | 0.64 | 0.44 | 0.69 |
| 42 | 0 | 900 | 969.84 | 9.83 | 437.07 | 13.85 | 1002.09 | 10.94 | 351.54 | 16.03 | 201.81 | 5.12 | 210.86 | 10.41 | 223.20 | 8.13 | 0.00 | 0.00 | 0.00 |
| 42 | 10 | 900 | 971.85 | 6.72 | 436.07 | 10.28 | 1004.27 | 7.87 | 354.58 | 8.42 | 201.53 | 3.37 | 211.39 | 7.71 | 223.36 | 6.40 | 0.40 | 0.34 | 0.61 |
| 42 | 30 | 900 | 971.96 | 6.04 | 436.26 | 9.88 | 1004.28 | 7.05 | 354.49 | 7.90 | 201.63 | 3.01 | 211.66 | 6.90 | 223.59 | 5.96 | 0.45 | 0.43 | 0.65 |
| 42 | 90 | 900 | 972.12 | 5.27 | 436.64 | 9.09 | 1004.49 | 6.52 | 354.67 | 7.57 | 201.77 | 2.72 | 212.05 | 6.23 | 223.83 | 5.55 | 0.54 | 0.49 | 0.68 |
| 43 | 0 | 900 | 968.23 | 10.79 | 436.77 | 16.19 | 1000.50 | 12.56 | 350.61 | 18.82 | 201.82 | 5.88 | 209.87 | 10.25 | 222.91 | 9.66 | 0.00 | 0.00 | 0.00 |
| 43 | 10 | 900 | 970.80 | 8.54 | 434.90 | 12.56 | 1002.34 | 9.20 | 353.58 | 10.24 | 201.46 | 3.69 | 210.79 | 10.02 | 223.04 | 7.79 | 0.32 | 0.32 | 0.56 |
| 43 | 30 | 900 | 972.06 | 7.25 | 435.93 | 10.85 | 1004.36 | 7.87 | 354.52 | 8.59 | 201.65 | 3.40 | 211.40 | 8.40 | 223.49 | 6.61 | 0.48 | 0.44 | 0.67 |
| 43 | 90 | 900 | 972.27 | 6.62 | 436.56 | 9.61 | 1004.81 | 7.30 | 354.84 | 7.95 | 201.74 | 2.95 | 211.86 | 7.79 | 223.74 | 6.02 | 0.59 | 0.49 | 0.71 |
| 44 | 0 | 900 | 970.20 | 9.32 | 436.95 | 12.49 | 1002.53 | 10.55 | 352.89 | 13.68 | 201.80 | 3.99 | 210.96 | 9.10 | 223.48 | 7.22 | 0.00 | 0.00 | 0.00 |
| 44 | 10 | 900 | 972.97 | 6.20 | 436.94 | 9.54 | 1005.75 | 7.02 | 355.41 | 7.37 | 201.87 | 2.71 | 212.32 | 7.24 | 224.00 | 5.27 | 0.39 | 0.41 | 0.63 |
| 44 | 30 | 900 | 972.68 | 5.02 | 436.72 | 8.63 | 1005.30 | 6.05 | 354.92 | 6.95 | 201.59 | 2.24 | 212.21 | 6.04 | 223.80 | 4.93 | 0.52 | 0.52 | 0.67 |
| 44 | 90 | 900 | 972.57 | 4.48 | 436.74 | 8.37 | 1005.08 | 5.69 | 354.70 | 6.74 | 201.55 | 2.17 | 212.34 | 5.40 | 223.84 | 4.82 | 0.55 | 0.56 | 0.69 |
| 44 | 300 | 900 | 972.11 | 5.25 | 436.33 | 8.83 | 1004.15 | 6.36 | 354.41 | 7.36 | 201.85 | 2.32 | 212.39 | 7.00 | 224.00 | 5.47 | 0.49 | 0.48 | 0.63 |
| 45 | 0 | 900 | 968.60 | 10.38 | 436.21 | 14.90 | 1000.39 | 11.72 | 351.02 | 16.08 | 201.57 | 5.41 | 210.14 | 10.76 | 222.96 | 8.37 | 0.00 | 0.00 | 0.00 |
| 45 | 10 | 900 | 972.59 | 6.80 | 436.49 | 10.02 | 1005.12 | 7.78 | 354.90 | 8.23 | 201.84 | 3.00 | 212.03 | 8.10 | 223.83 | 5.92 | 0.49 | 0.40 | 0.63 |
| 45 | 30 | 900 | 971.89 | 6.29 | 435.96 | 9.75 | 1004.06 | 7.48 | 354.23 | 8.36 | 201.55 | 2.85 | 211.65 | 7.31 | 223.55 | 5.84 | 0.52 | 0.43 | 0.62 |
| 45 | 90 | 900 | 971.42 | 5.62 | 435.65 | 9.76 | 1003.23 | 7.04 | 353.52 | 8.14 | 201.46 | 2.57 | 211.70 | 6.84 | 223.57 | 5.80 | 0.52 | 0.48 | 0.64 |
| 46 | 0 | 1000 | 968.39 | 10.94 | 436.34 | 15.59 | 1000.23 | 12.63 | 350.96 | 17.43 | 201.69 | 5.60 | 210.16 | 10.83 | 223.03 | 9.17 | 0.00 | 0.00 | 0.00 |
| 46 | 10 | 1000 | 973.48 | 3.66 | 437.69 | 6.86 | 1006.45 | 5.08 | 355.29 | 5.90 | 201.70 | 1.78 | 213.18 | 4.03 | 224.23 | 3.93 | 0.82 | 0.70 | 0.83 |
| 46 | 30 | 1000 | 972.67 | 3.75 | 437.31 | 7.48 | 1005.21 | 5.27 | 354.55 | 6.60 | 201.73 | 1.94 | 212.85 | 4.48 | 224.22 | 4.29 | 0.77 | 0.69 | 0.78 |
| 46 | 90 | 1000 | 973.42 | 3.11 | 437.91 | 6.54 | 1006.14 | 4.32 | 355.16 | 5.70 | 201.83 | 1.53 | 213.46 | 3.53 | 224.48 | 3.73 | 0.85 | 0.77 | 0.85 |
| 47 | 0 | 1000 | 964.40 | 16.29 | 434.72 | 24.18 | 995.43 | 18.67 | 347.31 | 26.71 | 201.31 | 7.16 | 207.48 | 21.36 | 222.32 | 11.79 | 0.00 | 0.00 | 0.00 |
| 47 | 10 | 1000 | 972.20 | 6.55 | 436.32 | 9.69 | 1004.59 | 7.29 | 354.61 | 7.95 | 201.72 | 2.98 | 211.72 | 7.35 | 223.72 | 6.02 | 0.76 | 0.68 | 0.81 |
| 47 | 30 | 1000 | 972.67 | 4.69 | 437.27 | 8.19 | 1005.36 | 6.30 | 354.77 | 7.24 | 201.83 | 2.42 | 212.52 | 5.64 | 224.15 | 4.87 | 0.83 | 0.74 | 0.84 |
| 47 | 90 | 1000 | 972.01 | 5.59 | 436.41 | 9.45 | 1003.99 | 6.92 | 354.12 | 7.89 | 201.81 | 2.75 | 212.09 | 6.80 | 223.98 | 5.81 | 0.77 | 0.70 | 0.81 |
| 48 | 0 | 1000 | 968.38 | 8.64 | 436.43 | 12.71 | 1000.30 | 10.60 | 351.36 | 14.90 | 201.59 | 5.85 | 210.51 | 9.35 | 223.08 | 8.28 | 0.00 | 0.00 | 0.00 |
| 48 | 10 | 1000 | 972.46 | 4.15 | 437.02 | 8.36 | 1004.89 | 5.75 | 354.57 | 6.91 | 201.68 | 2.21 | 212.49 | 5.10 | 224.03 | 4.73 | 0.56 | 0.56 | 0.71 |
| 48 | 30 | 1000 | 972.31 | 5.33 | 436.76 | 8.60 | 1004.83 | 6.33 | 354.56 | 7.40 | 201.81 | 2.42 | 212.22 | 6.24 | 223.98 | 5.41 | 0.53 | 0.49 | 0.66 |
| 48 | 90 | 1000 | 972.70 | 5.21 | 436.99 | 8.54 | 1005.34 | 6.08 | 355.16 | 6.95 | 201.90 | 2.38 | 212.37 | 6.14 | 224.18 | 5.22 | 0.54 | 0.52 | 0.70 |
| 48 | 300 | 1000 | 973.22 | 3.04 | 437.88 | 6.66 | 1005.98 | 4.46 | 355.02 | 5.85 | 201.83 | 1.63 | 213.27 | 3.99 | 224.43 | 3.83 | 0.78 | 0.71 | 0.80 |
| 48 | 1440 | 1000 | 973.16 | 3.25 | 437.72 | 6.93 | 1005.85 | 4.53 | 354.97 | 5.93 | 201.87 | 1.70 | 213.11 | 4.04 | 224.48 | 4.01 | 0.75 | 0.70 | 0.79 |
| 49 | 0 | 1000 | 968.26 | 9.61 | 436.30 | 11.63 | 1000.24 | 11.47 | 351.10 | 16.45 | 201.15 | 10.39 | 210.59 | 9.02 | 222.74 | 9.98 | 0.00 | 0.00 | 0.00 |
| 49 | 10 | 1000 | 971.81 | 6.73 | 436.06 | 10.10 | 1003.97 | 8.32 | 354.24 | 8.73 | 201.76 | 3.32 | 211.59 | 7.81 | 223.64 | 6.52 | 0.23 | 0.33 | 0.60 |
| 49 | 30 | 1000 | 972.10 | 7.41 | 436.05 | 10.01 | 1004.31 | 8.13 | 354.55 | 8.58 | 201.72 | 3.23 | 211.45 | 8.95 | 223.63 | 6.66 | 0.24 | 0.35 | 0.61 |
| 49 | 90 | 1000 | 972.25 | 6.50 | 436.36 | 9.58 | 1004.49 | 7.39 | 354.56 | 8.02 | 201.80 | 3.08 | 211.76 | 7.69 | 223.84 | 6.19 | 0.31 | 0.43 | 0.66 |
| 49 | 300 | 1000 | 971.82 | 4.74 | 436.46 | 8.59 | 1003.73 | 6.24 | 353.76 | 7.63 | 201.69 | 2.22 | 212.33 | 5.92 | 223.99 | 5.33 | 0.46 | 0.55 | 0.69 |
| 49 | 1440 | 1000 | 973.43 | 3.96 | 437.45 | 7.45 | 1006.12 | 4.85 | 355.27 | 5.95 | 201.86 | 1.88 | 212.87 | 4.86 | 224.31 | 4.39 | 0.63 | 0.69 | 0.82 |
| 50 | 0 | 1000 | 968.54 | 10.66 | 436.76 | 15.67 | 1000.69 | 11.98 | 351.07 | 17.83 | 201.79 | 6.13 | 210.18 | 11.10 | 223.06 | 9.43 | 0.00 | 0.00 | 0.00 |
| 50 | 10 | 1000 | 972.73 | 7.04 | 436.76 | 9.82 | 1005.67 | 7.09 | 354.97 | 8.14 | 201.93 | 2.87 | 212.50 | 9.50 | 223.93 | 6.14 | 0.55 | 0.49 | 0.68 |
| 50 | 30 | 1000 | 972.88 | 4.19 | 437.08 | 7.71 | 1005.52 | 5.51 | 355.12 | 6.46 | 201.66 | 2.01 | 212.92 | 5.80 | 224.03 | 4.54 | 0.75 | 0.64 | 0.80 |
| 50 | 90 | 1000 | 972.93 | 3.85 | 437.27 | 7.48 | 1005.50 | 5.05 | 355.07 | 6.48 | 201.80 | 1.85 | 213.12 | 5.21 | 224.22 | 4.38 | 0.77 | 0.69 | 0.80 |
| 50 | 300 | 1000 | 972.16 | 3.93 | 436.78 | 7.73 | 1004.52 | 5.02 | 354.11 | 6.52 | 201.73 | 1.63 | 212.94 | 4.90 | 224.20 | 4.46 | 0.74 | 0.69 | 0.79 |
| 50 | 1440 | 1000 | 973.53 | 3.30 | 437.76 | 6.67 | 1006.56 | 4.24 | 354.96 | 5.51 | 201.87 | 1.37 | 213.79 | 5.33 | 224.50 | 3.63 | 0.84 | 0.77 | 0.87 |
| 51 | 0 | 1000 | 967.98 | 10.40 | 437.16 | 15.85 | 1000.48 | 11.78 | 349.67 | 19.19 | 201.97 | 6.13 | 210.51 | 12.45 | 223.23 | 10.19 | 0.00 | 0.00 | 0.00 |
| 51 | 10 | 1000 | 972.60 | 7.04 | 436.62 | 10.06 | 1005.53 | 7.25 | 354.86 | 7.66 | 201.92 | 2.71 |  |  | 223.98 | 5.74 | 0.53 | 0.46 | 0.74 |
| 51 | 30 | 1000 | 972.29 | 6.24 | 436.42 | 9.44 | 1004.91 | 6.49 | 354.41 | 7.98 | 201.77 | 2.51 | 212.59 | 7.62 | 223.92 | 5.80 | 0.59 | 0.54 | 0.72 |
| 51 | 90 | 1000 | 972.63 | 4.59 | 437.26 | 7.73 | 1005.55 | 5.81 | 354.78 | 6.36 | 201.91 | 1.92 | 213.35 | 7.89 | 224.27 | 4.50 | 0.75 | 0.60 | 0.82 |
| 51 | 300 | 1000 | 970.77 | 5.28 | 435.21 | 10.06 | 1001.72 | 5.94 | 352.76 | 8.78 | 201.62 | 2.33 | 212.14 | 6.33 | 223.69 | 6.25 | 0.53 | 0.59 | 0.67 |
| 51 | 1440 | 1000 | 972.81 | 3.99 | 436.92 | 7.83 | 1004.89 | 4.94 | 354.54 | 6.43 | 201.83 | 1.66 | 212.99 | 5.73 | 224.31 | 4.41 | 0.74 | 0.69 | 0.82 |
| 52 | 0 | 1000 | 968.33 | 14.23 | 436.41 | 17.21 | 1000.21 | 15.13 | 350.57 | 20.19 | 201.90 | 6.95 | 210.56 | 12.27 | 222.97 | 9.86 | 0.00 | 0.00 | 0.00 |
| 52 | 10 | 1000 | 970.54 | 6.68 | 435.07 | 10.68 | 1001.87 | 8.73 | 352.97 | 9.67 | 201.47 | 3.17 | 211.23 | 8.56 | 223.30 | 7.02 | 0.53 | 0.48 | 0.63 |
| 52 | 30 | 1000 | 970.54 | 6.54 | 435.41 | 11.36 | 1001.71 | 7.47 | 352.86 | 9.55 | 201.62 | 2.98 | 211.65 | 7.70 | 223.59 | 6.86 | 0.48 | 0.58 | 0.64 |
| 52 | 90 | 1000 | 971.51 | 4.93 | 436.17 | 9.45 | 1003.04 | 5.97 | 353.94 | 8.00 | 201.79 | 2.48 | 212.10 | 5.95 | 223.92 | 5.92 | 0.64 | 0.69 | 0.73 |
| 53 | 0 | 1000 | 967.64 | 10.08 | 435.62 | 16.68 | 998.89 | 12.11 | 350.48 | 18.12 | 201.74 | 6.28 | 209.68 | 10.71 | 222.71 | 9.87 | 0.00 | 0.00 | 0.00 |
| 53 | 10 | 1000 | 972.03 | 6.87 | 436.02 | 9.72 | 1004.29 | 7.69 | 354.39 | 8.43 | 201.71 | 3.00 | 212.04 | 9.41 | 223.67 | 6.39 | 0.60 | 0.43 | 0.67 |
| 53 | 30 | 1000 | 970.43 | 6.71 | 434.96 | 11.35 | 1001.45 | 7.63 | 352.82 | 9.44 | 201.70 | 2.87 | 211.60 | 8.63 | 223.58 | 6.83 | 0.46 | 0.44 | 0.60 |
| 53 | 90 | 1000 | 972.19 | 5.30 | 436.53 | 9.13 | 1004.21 | 6.40 | 354.46 | 7.62 | 201.94 | 2.52 | 212.34 | 6.83 | 224.09 | 5.65 | 0.65 | 0.56 | 0.72 |
| 54 | 0 | 1000 | 968.60 | 9.82 | 436.58 | 15.33 | 1000.57 | 11.39 | 351.20 | 16.95 | 201.89 | 5.64 | 210.43 | 10.42 | 222.99 | 8.84 | 0.00 | 0.00 | 0.00 |
| 54 | 10 | 1000 | 971.89 | 5.42 | 436.27 | 9.47 | 1003.83 | 6.53 | 354.13 | 7.86 | 201.72 | 2.56 | 212.11 | 6.58 | 223.87 | 5.74 | 0.57 | 0.51 | 0.68 |
| 54 | 30 | 1000 | 972.87 | 3.83 | 437.30 | 7.78 | 1005.34 | 5.15 | 354.94 | 6.66 | 201.79 | 2.04 | 212.81 | 4.75 | 224.20 | 4.62 | 0.73 | 0.66 | 0.77 |
| 54 | 90 | 1000 | 971.81 | 4.61 | 436.61 | 8.60 | 1003.56 | 5.93 | 354.06 | 7.64 | 201.82 | 2.20 | 212.49 | 5.43 | 224.12 | 5.33 | 0.65 | 0.58 | 0.70 |
| 54 | 300 | 1000 | 972.09 | 4.06 | 436.69 | 8.26 | 1004.23 | 5.15 | 354.17 | 6.90 | 201.58 | 2.03 | 212.59 | 4.90 | 223.97 | 4.84 | 0.68 | 0.66 | 0.75 |
| 54 | 1440 | 1000 | 971.54 | 4.43 | 436.19 | 8.98 | 1002.89 | 5.59 | 353.60 | 7.67 | 201.83 | 2.13 | 212.39 | 5.26 | 224.10 | 5.34 | 0.61 | 0.61 | 0.70 |
| 55 | 0 | 1000 | 968.83 | 9.18 | 436.31 | 14.77 | 1000.57 | 10.79 | 351.32 | 15.40 | 201.82 | 4.90 | 210.65 | 11.14 | 223.17 | 8.38 | 0.00 | 0.00 | 0.00 |
| 55 | 10 | 1000 | 971.35 | 7.09 | 435.50 | 10.99 | 1002.95 | 7.71 | 353.80 | 8.88 | 201.71 | 2.96 | 211.63 | 8.39 | 223.60 | 6.55 | 0.39 | 0.35 | 0.55 |
| 55 | 30 | 1000 | 971.70 | 5.75 | 435.94 | 9.82 | 1003.32 | 6.62 | 353.85 | 8.21 | 201.74 | 2.56 | 212.12 | 6.94 | 223.85 | 5.78 | 0.51 | 0.47 | 0.61 |
| 55 | 90 | 1000 | 972.49 | 4.44 | 437.02 | 8.28 | 1004.63 | 5.76 | 354.44 | 7.23 | 201.82 | 2.13 | 212.74 | 5.41 | 224.18 | 5.00 | 0.66 | 0.57 | 0.69 |
| 55 | 300 | 1000 | 972.20 | 3.71 | 436.85 | 8.10 | 1004.09 | 4.87 | 354.15 | 6.92 | 201.80 | 1.97 | 212.71 | 4.57 | 224.21 | 4.85 | 0.68 | 0.67 | 0.72 |
| 55 | 1440 | 1000 | 973.93 | 3.10 | 438.02 | 6.61 | 1006.81 | 3.82 | 355.61 | 5.37 | 201.92 | 1.47 | 213.55 | 3.74 | 224.59 | 3.70 | 0.84 | 0.78 | 0.85 |
| synthetic | - | - | 974.66 | 2.12 | 438.38 | 4.98 | 1008.18 | 1.90 | 356.21 | 3.61 | 201.83 | 0.31 | 214.67 | 1.70 | 224.84 | 2.16 | - | - | - |

Supplementary Table S3. Mean fractions of annealing of the isothermal runs for the ν2(SiO4), ν3(SiO4), and external rotation band (ER).

| T [°C] | t [min] | ln(t) [ln(s)] | 10000/T [1/K] | Mean Φ3 | Mean Φ2 | Mean ΦER |
| --- | --- | --- | --- | --- | --- | --- |
| 500 | 30 | 7.50 | 12.94 | 0.14 | 0.24 | 0.27 |
| 500 | 90 | 8.59 | 12.94 | 0.15 | 0.22 | 0.35 |
| 500 | 300 | 9.80 | 12.94 | 0.22 | 0.24 | 0.36 |
| 500 | 1440 | 11.37 | 12.94 | 0.22 | 0.25 | 0.39 |
| 600 | 10 | 6.40 | 11.45 | 0.13 | 0.1 | 0.23 |
| 600 | 30 | 7.50 | 11.45 | 0.24 | 0.21 | 0.39 |
| 600 | 90 | 8.59 | 11.45 | 0.25 | 0.23 | 0.41 |
| 600 | 300 | 9.80 | 11.45 | 0.29 | 0.27 | 0.46 |
| 600 | 1440 | 11.37 | 11.45 | 0.36 | 0.33 | 0.52 |
| 600 | 7200 | 12.98 | 11.45 | 0.35 | 0.32 | 0.50 |
| 700 | 10 | 6.40 | 10.28 | 0.17 | 0.22 | 0.40 |
| 700 | 30 | 7.50 | 10.28 | 0.30 | 0.29 | 0.54 |
| 700 | 90 | 8.59 | 10.28 | 0.26 | 0.29 | 0.52 |
| 700 | 300 | 9.80 | 10.28 | 0.30 | 0.31 | 0.55 |
| 700 | 1440 | 11.37 | 10.28 | 0.35 | 0.41 | 0.59 |
| 700 | 7200 | 12.98 | 10.28 | 0.36 | 0.40 | 0.61 |
| 800 | 10 | 6.40 | 9.32 | 0.39 | 0.40 | 0.58 |
| 800 | 30 | 7.50 | 9.32 | 0.42 | 0.42 | 0.61 |
| 800 | 90 | 8.59 | 9.32 | 0.45 | 0.47 | 0.63 |
| 800 | 300 | 9.80 | 9.32 | 0.49 | 0.54 | 0.66 |
| 800 | 1440 | 11.37 | 9.32 | 0.55 | 0.62 | 0.70 |
| 800 | 7200 | 12.98 | 9.32 | 0.58 | 0.63 | 0.70 |
| 900 | 10 | 6.40 | 8.53 | 0.39 | 0.44 | 0.62 |
| 900 | 30 | 7.50 | 8.53 | 0.43 | 0.50 | 0.65 |
| 900 | 90 | 8.59 | 8.53 | 0.49 | 0.56 | 0.68 |
| 900 | 300 | 9.80 | 8.53 | 0.60 | 0.66 | 0.74 |
| 1000 | 10 | 6.40 | 7.86 | 0.50 | 0.55 | 0.69 |
| 1000 | 30 | 7.50 | 7.86 | 0.56 | 0.59 | 0.70 |
| 1000 | 90 | 8.59 | 7.86 | 0.61 | 0.66 | 0.75 |
| 1000 | 300 | 9.80 | 7.86 | 0.65 | 0.65 | 0.74 |
| 1000 | 1440 | 11.37 | 7.86 | 0.70 | 0.74 | 0.81 |